OPTIMIZATION OF MATERIAL REMOVAL RATE IN EDM OF MILD STEEL

A MAJOR PROJECT REPORT

SUBMITTED AS PARTIAL FULFILLMENT OF THE REQUIREMENT

FOR THE AWARD OF DEGREE OF

MASTER OF ENGINEERING

IN

PRODUCTION ENGINEERING

SUBMITTED BY

MANJEET KUMAR

(UNIVERSITY ROLL NO. 8523)

UNDER THE GUIDANCE OF

DR. (Mrs.) REETA WATTAL

DEPARTMENT OF MECHANICAL AND PRODUCTION ENGINEERING

DELHI COLLEGE OF ENGINEERING

UNIVERSITY OF DELHI, DELHI-110042

SESSION 2009-10

Candidate Declaration

I, MANJEET KUMAR, hereby certify that the work which is being presented in the thesis entitled “Optimization of material removal rate in EDM of mild steel”. in the partial fulfillment of requirement for the award of degree of MASTER OF ENGINEERING submitted in the Department of Mechanical Engineering at DELHI COLLEGE OF ENGINEERING under UNIVERSITY OF DELHI, DELHI, is an authentic record of my own work carried out during a period from July 2009 to July 2010, under the supervision of Dr. (Mrs.) Reeta Wattal (Department of Mechanical engineering). The matter presented in this thesis has not been submitted in any other University / Institute for the award of any degree.

(Manjeet kumar)

University Roll No: 8523

This is to certify that the above statement made by the candidate is true to the best of my knowledge.

Dr. REETA WATTAL

Assistant Professor

Department of Production and Industrial Engineering

Delhi College of Engineering,

Delhi-110042 (India)

Acknowledgement

I wish to acknowledge my profound sense of gratitude to my project Guide Dr. Reeta Wattal, Assistant professor, Department of Production and Industrial Engineering, Delhi College of Engineering, Delhi for her remarkable guidance and many valuable ideas during the preparation of this project. Indeed it was a matter of great felicity and privilege for me to work under her aegis was express my thankfulness to her for her dedicated inspiration, lively interest and patience through my errors with which it would have being impossible to bring the project near completion.

I wish to extend my hearty thanks to Mr. Pradeep kumar, head of mechanical work shop who helped me in this project work. I would also like to thank the management of the workshop for their useful contribution.

I wish to extend my hearty thanks to all the staff of the department who directly or indirectly helped me in this project work.

And lastly I express sincere gratitude to Prof. B.D. Pathak HoD, Department of Mechanical Engineering, Prof. S.K.Garg, HoD Training and Placement with whose blessing this project was completed.

Manjeet Kumar

University Roll No. 8523

Department of Production Engineering

Delhi College of Engineering, New Delhi

2008-2010

OPTIMIZATION OF MRR IN EDM OF

MILD STEEL

abstract

The present work compiled in this thesis aims at achieving the integrated approach to solve the optimization problem of EDM process. At any stage, the dominance factor of the input variables and output variables contained in the constraints and objective functions can be computed. This technique helps in getting the reliable multi-objective decisions under constrained penalties for the constrained optimization of such processes.

In the present work, relationships have been developed between the input decision variables and the desired goals by applying the statistical regression analysis of investigations obtained by Electro Discharge machining process for a considerable variation in the crisp sets of variables. The objectives functions were maximized or minimized by using the generalized Genetic Algorithms and the data are stored for a given set of objectives. The results are interpreted with respect to those obtained by using the bi-criterion approach. It is concluded that the results obtained by bi-criterion approach are approximately of the same order of accuracy as calculated experimentally but the computational simplicity of this method makes this methodology favorable to use to solve such mechanical engineering complex problems.

index

Chapter no.

- Introduction

  - Introduction

  - Electric Discharge Machining

  - Optimization

  - Need of optimization in production

  - Goal programming

  - Research and Methodology

  - Motivation and objectives

  - Conclusion

- Literature Review

  - Introduction

  - Literature Review

  - Conclusion

- Optimization

  - Introduction

  - Literature Review of traditional optimization techniques

  - Optimization techniques

    - Fuzzy logic

    - Genetic algorithm (GA)

    - Scatter search technique(SS)

    - Taguchi technique

    - Response surface methodology(RSM)

  - Conclusion

- Multiple criteria decision making

  - Introduction

  - Multiple criteria decision making methods

    - Non-compensatory methods

    - Compensatory methods

  - Applications of MCDM

  - Conclusion

- Electric discharge machining

  - Introduction

  - Parameters affecting EDM process

  - Process parameters

  - Dielectric fluid

  - Spark gap

  - Description of EDM controls

  - Experimental Procedure

- Optimization of material removal rate

  - Introduction

  - Constraints

  - Mathematical analysis

- Results analysis and discussion

  - Effect of current on surface roughness

  - Effect of current on material removal rate

  - Optimization analysis

- Conclusion and future scope

REFERENCES

LIST OF SYMBOLS

P			: Dielectric Pressure, hPa

N			: Power consumption by machine in Watts

Q			: Metal removal rate in mm3/min

Δ			: Electrode wear in percentage

Ti			: Pulse duration in Seconds

To			: Pulse interval time in Seconds

I			: Discharge current in Amperes

Φ			: erosion diameter in mm

V			: Applied working voltage in Volts

G			: Erosion depth in mm

Ra			: Surface roughness in Meters

Ω,Δ			: modified Chebyshev Goal programming Objective

Functions

≤,±,≥			: Mathematical operators

LIST OF FIGURES AND TABLES

Fig 5.1 Action of spark between electrode and work-piece

Fig 5.2 Basic EDM processes

Fig 5.3 controller of EDM (SPARKONIX A-35)

Fig. 5.4 to check level of the lower surface of copper electrode

Fig. 5.5 Setup of work-piece & electrode

Fig. 5.6 Work-piece for final analysis

Table 5.1 Specification of machine

Table 5.2 Parameters for experiments

Table 5.3 Surface roughness at various values of current

Table 5.4 Material removal rate at various values of current

Graph 5.1a Effect of current on surface roughness

Graph 5.1b Effect of current on material removal rate