EFFECT OF CURRENT ON MATERIAL REMOVAL RATE WITH DIFFERENT ELECTRODES INEDM

A MINOR PROJECT REPORT

SUBMITTED AS PARTIAL FULFILLMENT OF THE REQUIREMENT

FOR THE AWARD OF DEGREE OF

MASTER OF ENGINEERING

IN

PRODUCTION ENGINEERING

SUBMITTED BY

MANJEET KUMAR

(UNIVERSITY ROLL NO. 8523 )

UNDER THE GUIDANCE OF

DR. (Mrs.) REETA WATTAL

DEPARTMENT OF MECHANICAL AND PRODUCTION ENGINEERING

DELHI COLLEGE OF ENGINEERING

UNIVERSITY OF DELHI, DELHI-110042

SESSION 2009-10

Candidate Declaration

I, MANJEET KUMAR, hereby certify that the work which is being presented in the thesis entitled “EFFECT OF CURRENT ON MATERIAL REMOVAL RATE WITH DIFFERENT ELECTRODES IN EDM”. in the partial fulfillment of requirement for the award of degree of MASTER OF ENGINEERING submitted in the Department of Mechanical Engineering at DELHI COLLEGE OF ENGINEERING under UNIVERSITY OF DELHI, DELHI, is an authentic record of my own work carried out during a period from July 2009 to July 2010, under the supervision of Dr. (Mrs.) ReetaWattal(Department of Mechanical engineering). The matter presented in this thesis has not been submitted in any other University / Institute for the award of any degree.

(Manjeetkumar)

University Roll No: 8523

This is to certify that the above statement made by the candidate is true to the best of my knowledge.

Dr. REETA WATTAL

Assistant Professor

Department of Production and Industrial Engineering

Delhi College of Engineering,

Delhi-110042 (India)

Acknowledgement

I wish to acknowledge my profound sense of gratitude to my project Guide Dr. ReetaWattal, Assistant professor, Department of Production and Industrial Engineering, Delhi College of Engineering, Delhi for her remarkable guidance and many valuable ideas during the preparation of this project. Indeed it was a matter of great felicity and privilege for me to work under her aegis was express my thankfulness to her for her dedicated inspiration, lively interest and patience through my errors with which it would have being impossible to bring the project near completion.

I wish to extend my hearty thanks to Mr. Pradeepkumar, head of mechanical work shop who helped me in this project work. I would also like to thank the management of the workshop for their useful contribution.

I wish to extend my hearty thanks to all the staff of the department who directly or indirectly helped me in this project work.

And lastly I express sincere gratitude to Prof. B.D. PathakHoD, Department of Mechanical Engineering, Prof. S.K.Garg,HoD Training and Placement with whose blessing this project was completed.

Manjeet Kumar

University Roll No. 8523

Department of Production Engineering

Delhi College of Engineering, New Delhi

2008-2010

Delhi-110042 (India)

EFFECT OF CURRENT ON MATERIAL REMOVAL RATE WITH DIFFERENT ELECTRODES IN EDM

abstract

Electrical discharge machining (EDM) is one of the earliest nontraditional machining processes. EDM process is based on thermo electric energy between the work piece and an electrode. A pulse discharge occurs in a small gap between the work piece and the electrode and removes the unwanted material from the parent metal through melting and vaporizing. The electrode and the work piece must have electrical conductivity in order to generate the spark. This paper review’s the effect of current on material removal rate with different electrode.

In thesis work literature has been studied in context to modeling of EDM. The equation of MRR and surface finish has been developed in order to attain target and optimum results.

The approach of optimum and modeling of MRR and surface finish for batch production has been applied becausenow days, manyindustryare following batchproduction. The optimum value has been determined with the help of S/N ratio. The optimum value has been determined which is suitable for both MRR and surface finish.

TABLE OF CONTENTS

CHAPTER NO

- Introduction

  - Introduction

  - Process parameters

  - Material removal rate

  - Surface finish

  - Conclusion

- Literature review

  - Introduction

  - Review of literature view

  - Conclusion

- Electric Discharge Machining

  - Introduction

  - Spark erosion machining process

  - Working principle of EDM process

  - Spark erosion generators

  - Electrode feed controller

  - Process parameters

  - Dielectric fluids

  - Flushing

- Effect of current on MRR & surface finish

  - Introduction

  - Objective of work

  - Experimental procedure

  - Analyzing MRR & surface roughness by S/N method

  - Confirmation test

  - Limitation

  - Conclusion

- Result analysis and discussion

  - Effect of current on surface roughness

  - Effect of current on material removal rate

- Conclusion and future scope

REFRENCES

LIST OF FIGURES AND TABLES

Fig: 3.1 Process of sinking by EDM

Fig: 3.2 Cutting by EDM

Fig: 3.3 Grinding by EDM

Fig 3.4 Setup for EDM

Fig 3.5 Relaxation circuit

Fig 3.6 Effect of current on surface

Fig 3.7 Concept of pulse on time and pulse off time

Fig 3.8 Frequency setting

Fig. 4.1Check level of lower surface of the electrode

Fig. 4.2 Setup of work piece & electrode

Fig. 4.3 Work piece for final analysis

Table 3.1 Recommended polarities for different tool-job pair

Table 4.1 Machining parameters

Table 4.2 Specification of machine

Table 4.3 Parameters for experiment

Table 4.4 Surface roughness at various values of current with Al electrode

Table 4.5 Material removal rate at various values of current with Al electrode

Table 4.6 Surface roughness at various values of current with Cu electrode

Table 4.7 Material removal rate at various values of current with Cu electrode

Table 4.8 S/N ratios of MRR and surface roughness

Graph 4.1a Effect of current on surface roughness with Al electrode

Graph 4.1b Effect of current on material removal rate with Al electrode

Graph 4.1c Effect of current on surface roughness with Cu electrode

Graph 4.1d Effect of current on material removal rate with Cu electrode