STUDY OF RECYCLED POLYETHYLENE AND POLYPROPYLENE

A major project submitted in the partial fulfillment of the requirement for the award of the Degree of

Master of Engineering

In

Polymer Technology

In the Faculty of Technology,

University of Delhi, Delhi

By

MOHAN SINGH RAWAT

(10/Poly/03)

Under the guidance of

Dr. D. Kumar

DEPARTMENT OF APPLIED CHEMISTRY

& POLYMER TECHNOLOGY,

DELHI COLLEGE OF ENGINEERING

DELHI-110042

JUNE-2006

DEPARTMENT OF APPLIED CHEMISTRY & POLYMER TECHNOLOGY

DELHI COLLEGE OF ENGINEERING, DELHI

CERTIFICATE

This is to certify that Mr. Mohan Singh Rawat has satisfactorily completed the project work entitled “Study of recycled polyethylene and polypropylene” in partial fulfillment of the requirement for the award of the Degree of Master of Engineering in Polymer Technology of Delhi College of Engineering, Delhi during the academic session 2005-2006.This work has not been submitted in part or full in any other university or institution for the award of any other degree or diploma.

Dr. D.Kumar					         Prof.G.L.Verma

(Asstt. Professor)                                                     Head,

Department of Applied Chemistry		          Department of Applied Chemistry	                 Delhi College of Engineering, Delhi		          Delhi College of Engineering, Delhi

Acknowledgement

Although, it is practically impossible to acknowledge the help and guidance of every one who has assisted me during this project work, there are a number of people whom credit must be given. My work would never have been possible with out one person. So, I express  my   profound   sense  of   gratitude,  humble  indebtness  and  sincere  thanks  to

Dr. D. Kumar, Assistant professor, Department of Applied Chemistry and Polymer Technology, Delhi College of Engineering, for his guidance, constant encouragement, suitable help and intellectual inspiration throughout my project work.

I am extremely grateful to Prof. G. L.Verma, Head, Department of Applied Chemistry & Polymer Technology, Delhi College of Engineering, Delhi, for inspiration and encouragement. I express my thanks whole heartily to Dr. A. P. Gupta., Dr. R. C. Sharma, Dr. Archana Rani, Mrs. V.K.Smitha and Mr. S.G. Warker.

I am also thankful to the Lab staff, Department of Applied Chemistry & Polymer Technology, Delhi College of Engineering, Delhi, for their invaluable support.

Words  are  inadequate  to  express  my  regards  and thanks  to   my  family  especially  to  Mrs. Era Rawat, who always stands by me in times of need.

Last but not the least, I heartily acknowledge my friends and my colleagues for their help, encouragement and discipline during the entire project work.

Date:

Place: Delhi                                                                     (MOHAN SINGH RAWAT)

LIST OF CONTENTS

Chapter No.	 						         	Page No.

ABSTRACT									i

LIST OF FIGURES								ii

LIST OF TABLES								iii

LIST OF GRAPHS								v

1.        INTRODUCTION								1

Why plastics are recycled?							2

Brief overview of polyethylene	       					5

Brief overview of polypropylene						9

Brief overview of PET & PS							14

Production & consumption scenario of plastics in India			16

Collection of plastic waste							19

Transportation of plastic waste			             		21

Recycling of plastic waste							23

Degradation of plastics during recycling					31

Effect of recycling on properties of plastics					36

Processing of plastic waste					 		37

Manufacturing process for recycled waste					42

Testing process of recycled plastic waste					45

- EXPERIMENTAL DETAILS

Raw material used       								46

Sample preparation for testing							47          Physical properties								49

- Specific gravity test

- Shore D hardness test

Mechanical properties								51

- Tensile properties

- Flexural properties

- Impact test

Thermal analysis								55

- Heat deflection temperature

- Melt flow index test

3.        RESULTS & DISCUSSION							58

4.        CONCLUSION & FUTURE ASPECTS					70

REFFERENCES								72

ABSTRACT

The project aims to study the complete procedure followed for recycling of plastic waste, i.e., collection of waste scrap of plastic, transportation of this waste to the recycling centers, different processing parameters and finally the testing of waste and recycled samples. Further comparative study between waste and recycled polyethylene (high density polyethylene) and polypropylene was also carried out.

The study is concerned with analyzing the collection, transportation, processing & testing of recyclable polymeric materials, i.e., polyethylene and polypropylene. Polyethylene and polypropylene are chosen here as recyclable materials. Extrusion process was chosen to observe the effect of recycling/ reprocessing. For comparative study between waste and recycled polyethylene and polypropylene, the effect was seen up to two processing cycles. There was a marginal decrease in physical and mechanical properties. There was a small increase in melt flow index while heat deflection temperature has showed decreasing trends.

The overall analysis of results suggested that recycling/reprocessing was not severe on physical and mechanical properties of polyethylene and polypropylene waste. Thus, recycling would be an ideal step to meet the increasing demand of material, conservation of natural resources and plastic waste management.

(i)

LIST OF FIGURES

Figure No.		Captions						   Page No.

Fig. 1			Blocks of actactic and isotactic polypropylene		 11

in same polymer chain

Fig. 2			Hard clumps of crystalline isotactic polypropylene		 12

tied together by rubbery tethers of atactic polypropylene

Fig. 3(a)		Collection of plastic waste					 38

Fig. 3(b)		Sorting of waste plastic					 38

Fig. 4			Flow chart of a typical waste plastic reprocessing stream	 39

Fig. 5			Extrusion machine						 43

Fig. 6			Injection moulding machine					 44

Fig. 7			Blow moulding machine					 44

(ii)

LIST OF TABLES

Table No.		Captions				    		Page No.

- Polymer demand in India		   			16

- Year wise data on consumption & plastics

waste available for recycling					17

- Consumption of PE, PP & PET during year 2001		18

- Application of PE, PP & PET during year 2001		18

- Demand scenario of PE, PP & PET in India			19

- Resin identification coding system				28

- Commercial uses of virgin & recycled plastics		29

- Simple test for recognization of plastics			45

- Processing parameters for HDPE & PP			47

10			Processing parameters for compression moulding		48

11			Dimensions of test specimens for tensile properties		52

12			Dimensions of test specimens for flexural properties		53

13  			Dimensions of test specimens for impact test			55

14			Dimensions of test specimens for measurement of HDT	55

15			Comparison of specific gravity of different samples		58

16			Comparison of hardness of different samples			59

(iii)

17			Tensile strength and tensile modulus of different samples

of HDPE and PP						60

- Comparison of  flexural strength and modulus of

different samples of HDPE and PP				62

- Comparison of  impact strength of different samples

of HDPE and PP						64

20			Comparison of  HDT for HDPE and PP samples		65

21			Comparison of  MFI of  HDPE and PP samples		67

(iv)

LIST OF GRAPHS

Table No.		Captions						   Page No.

1		          Polymer demand in India					17

2		            Histogram representing tensile strength of HDPE and

PP samples							61

3		            Histogram representing tensile modulus of HDPE and

PP samples							61

4			Histogram representing flexural strength of HDPE and

PP samples							63

5		            Histogram representing flexural modulus of HDPE and

PP samples		                                                          	63

6		           Histogram representing impact strength of HDPE and

PP samples							65

7                           Variation of heat deflection temperature of HDPE

sample series							66

8                           Variation of heat deflection temperature of  PP

samples series							67

9                           Variation of melt flow index of HDPE samples		68

10                         Variation of melt flow index of PP samples			69

(v)