MATHEMATICAL MODELLING OF SURFACE ROUGHNESS IN TURNING OF EN8 WITH CARBIDE TOOL

#### A Major Project thesis Submitted in partial fulfillment for the requirement for the award of the degree of

Masters of Engineering

in

Production and Industrial Engineering

Submitted By:

Saadat Ali Rizvi

University Roll No. 50322

College Roll No.019/Prod/05

Under the guidance of

Dr. VIPIN

Asstt. Prof.

DEPARTMENT OF MECHANICAL ENGINEERING

DELHI COLLEGE OF ENGINEERING

DELHI UNIVERSITY, DELHI-110042

June, 2008

Candidate’s declaration

I, SAADAT ALI RIZVI hereby certify that the work which is being presented in this thesis entitled “MATHEMATICAL MODELLING OF SURFACE ROUGHNESS IN TURNING OF EN8 WITH CARBIDE TOOL” in the partial fulfillment of requirement for the award of degree of Masters of Engineering submitted in the Department of Mechanical Engineering at Delhi College Of Engineering, is an authentic record of my own work carried out during a period from July 2005 to June 2008, under the supervision of Dr. VIPIN, Asstt. Prof. Department of Mechanical Engineering, Delhi College of Engineering, Delhi.

The matter presented in this thesis has not been submitted in any other University/ Institute for the award of M.E. Degree.

Signature of the Student

(Saadat Ali Rizvi)

CERTIFICATE

This is to certify that the above statement made by the candidate is correct to best of my knowledge.

Signature of the Guide

(Dr. VIPIN)

ACKNOWLEDGEMENT

It is a matter of great pleasure for me to present my dissertation report on “MATHEMATICAL MODELLING OF SURFACE ROUGHNESS IN TURNING OF EN8 WITH CARBIDE TOOL”. First and foremost, I am profoundly grateful to my guide Dr. VIPIN, Asst. Prof, Mechanical Engineering Department for his expert guidance and continuous encouragement during all stages of thesis. I feel lucky to get an opportunity to work with him. Not only understanding the subject, but also interpreting the results drawn thereon from the graphs was very thought provoking. I am thankful to the kindness and generosity shown by him towards me, as it helped me morally complete the project before actually starting it.

I would like to thank Er. S.K Verma, Managing Director, Gauri Components (P) Ltd., Meerut (UP), Er Sunder, Er Wajahat Ali and special thanks to Er. Vineet Kumar Saxena, Coordinator of SCRIET (CCS University, Meerut) and  Sh. Rahul Mool (Metrology Lab., In charge of DCE) without their support it would be almost impossible to complete my thesis work in time.

Last, but not the least, I would like to thank my family members specially my wife for their help, encouragement and prayers through all these months. I dedicate my work to them.

Date:

Place:

Saadat Ali Rizvi

CONTENTS

CANDIDATE’S DECLARATION							2

ACKNOWLEDGEMENT								3

ABSTRACT										9

Chapter 1: INTRODUCTION								10-13

### 1.1      Introduction								9

### 1.2      Types of Roughness							10

1.2.1 Ideal Roughness							10

1.2.2 Natural Roughness 							11

1.3      Cutting Parameters								11		1.3.1 Cutting Speed								11

1.3.2 Feed 								12

1.3.3 Depth of Cut							12

1.3.4 Effect of Cutting Parameters					12

1.3.5 Nose radius							12

Chapter 2: LITERATURE REVIEW					           		 14-19

Chapter 3: REGRESSION AND DESIGN OF EXPERIMENTS		 	20-34

  - Regression Analysis							20

    - Linear Regression						20

    - Non-Linear Regression						21

    - Analysis Technique						22

      - Least Square analysis					26

      - Model Assumptions					27

      - Model Validity						19

  - Design Of Experiments							30

    - Concept of DOE						31

    - Problem Identification						33

    - Taguchi’s Parameter Design Method				34

      - Objectives of Taguchi’s Method			34

      - Orthogonal Array					34

    - Brainstorming							35

    - Types of Optimization Problems					37

      - Static Problems						37

      - Dynamic Problems					38

    - Batch Process Optimization					39

      - Smaller the Better					39

      - Larger the Better					39

      - Nominal the Best					39

    - Steps in Taguchi Methodology					40

    - Advantages of Taguchi Design of Experiment			42

    - Limitations of	 Taguchi Design of Experiment			42

Chapter 4: EXPERIMENTAL SET UP						44-59

  - CNC  Lathe Machine							44

  - System Configuration							45

  - Surface Roughness Measuring Instrument					49

  - Work-piece material							55

  - Cutting tool material 							56

  - Measurement of Surface Roughness					57

    - Direct Measurement Methods					57

    - Comparison Based Techniques					58

    - Non Contact methods						58

  - Factors and their levels			   				59

Chapter 5: ANALYSIS OF MACHINING DATA					60-70

5.1 Mathematical Models Formulation of Machining Data			60

    - Non-Linear Model 						60

    - Surface roughness Equation					69

Chapter 5:  RESULTS AND CONCLUSION 				  		70-75

REFERENCES							 	76-79

APPENDIX								 80-83

BIBLOGRAPHY								84-89

List of Tables

Table No	Table Description					                                 Page

4.1		CNC lathe Machine specifications				      	47

4.2		Chemical Composition of Work Piece 			      		56

4.3		Process Parameters and their Levels				      	59

5.1		Data Collection for Model			      			64

5.2		Result of Regression Analysis 			      			66

6.1    		Compression of Actual and Calculated surface roughness		72

ABSTRACT

Turning is one of the most widely used metal cutting processes. The increasing importance of turning operations is gaining new dimensions in the present industrial age, in which the growing competition calls for all the efforts to be directed towards the economical manufacture of machined parts as well as surface finish is one of the most critical quality measure in mechanical products. In present work, a Regression Analysis is adopted to construct a prediction model for surface roughness. Once the process parameters (cutting speed, feed, depth of cut, Nose Radius and Speed) are given, the surface roughness can be predicted.

The work piece material is EN8 which is processed by carbide-inserted tool. All the experiment work is conducted on CNC lathe. The experiments are carried out by using design of experiment. Regression analysis is done considering Non-Linear model.  Finally the contributions are summarized and future research directions are highlighted.

Chapter 1

INTRODUCTION

Todays manufacturing industries are very much concerned about the quality of their products. They are focused on producing high quality products in time at minimum cost. Surface Roughness (finish) is one of the crucial performance parameters that have to be controlled within suitable limits for a particular process. Therefore, prediction or monitoring of the surface roughness of machined components has been an important area of research. Surface roughness is harder to attain and track than physical dimensions are, because relatively many factors affect surface roughness. Some of these factors can be controlled and some cannot. Controllable process parameters include feed, cutting speed, tool geometry, nose radius and tool setup. Other factors, such as tool, work piece and machine vibration, tool wear and degradation, and work piece and tool material variability can not be controlled as easily.

Surface roughness also affects several functional attributes of parts, such as contact causing surface friction, wearing, light reflection, heat transmission, ability of distributing and holding a lubricant, coating or resisting fatigue. Therefore the desired finish surface is usually specified and the appropriate are selected to reach the required quality.

Several works have been reported in the broad field of tool condition monitoring. Researchers are trying to develop a robust and accurate model that can find a correlation between the cutting parameters and the surface roughness of the machined products.

1.1 Types of Roughness

The resultant roughness produced by a machining process can be thought of as the combination of two independent effects: Ideal roughness and Natural roughness.

### 1.1.1 Ideal Roughness

Ideal surface roughness is a function of only feed and geometry. It represents the best possible finish which can be obtained for a given tool shape and feed. It can be achieved only if the built-up-edge, chatter and inaccuracies in the machine tool movements are eliminated completely. For a sharp tool without nose radius, the maximum height of unevenness is given by:

### R max = f / (cot φ + cot β)

Ra = Rmax / 4

Fig. 1.1 Ideal roughness Geometry

f   Feed

Ф  Major cutting edge angle

Β  working minor cutting edge angle

1.1.2 Natural Roughness

In practice, it is not usually possible to achieve conditions such as those described above, and normally the natural surface roughness forms a large proportion of the actual roughness. One of the main factors contributing to natural roughness is the occurrence of a built-up edge. Thus, larger the built up edge, the rougher would be the surface produced, and factors tending to reduce chip-tool friction and to eliminate or reduce the built-up edge would give improved surface finish.

Surface roughness of machined surfaces

Surface roughness is caused by:

- The feed marked or ridges left by the cutting tool, and

- The fragments of built-up edge shed on the work surface in the process of chip formation. Surface finish can be improved by reducing the height of the feed ridges and the size of the built up edge.

1.2 Cutting Parameters

The important cutting parameters discussed here are cutting speed, feed, nose radius and depth of cut.

1.2.1 Cutting Speed

All materials have an optimum Cutting Speed and it is defined as the speed at which a point on the surface of the work passes the cutting edge or point of the tool and is normally given in meters/min. To calculate the spindle Speed required,

N= 1000 VC /Dπ

Where: 
N = Spindle Speed (RPM), VC = Cutting Speed of Metal (m/min), D = Diameter of W/p

1.2.2 Feed

The term `feed' is used to describe the distance the tool moves per revolution of the work piece and depends largely on the surface finish required. For roughing out a soft material a feed of up to 0.25 mm per revolution may be used. With tougher materials this should be reduced to a maximum of 0.10 mm/rev. Finishing requires a finer feed then what is recommended.

1.2.3 Depth of cut
it is the advancement of tool in the job in a direction perpendicular to the surface being machined. Depth of cut depends upon cutting speed, rigidity of machine tool and tool material etc. Depth of cut normally varies between 1 to 5 mm for roughing operation and 0.2 to 1 mm for finishing operation.

1.2.3.4 Nose Radius

1.2.4 Effect of cutting parameters

It is found in most of the cases surface roughness decreases with increase in cutting speed and decrease in feed and depth of cut.

Since these cutting parameters will decide about the type of chips which we expect at the time of machining of a single constant material thus we have to analyze them for no such built-up edge chips formation. At the optimum cutting speed at which the effect of built up edge is negligible, (high speed, ductile material) the profile of the cutting edge of the tool is reproduced on the work surface and this ideal surface roughness is mainly dependent on cutting feed. That means for a greater feed the average roughness value is more as compared to the lesser feed.

It would be noted that the size of chips cross-sectional area has a large effect on surface finish. Surface finish is poor for large cuts which is desirable from considerable of high tool life and power consumption. Large feed is more detrimental to surface finish than a large depth of cut.

For very high cutting speeds the chances of built up edge reduces thus surface roughness also expected to reduce, while when cutting speed is low built-up formation of chips would increase the surface roughness.

Chapter 2

LITERATURE REVIEW

A considerable number of studies have investigated the general effects of the speed, feed, and depth of cut, nose radius and others on the surface roughness. These studies have been briefly discussed for the variations observed experimentally.

- M.Cemal cakir, Chiat Ensarioglu, llker Demirayak developed a regression Analysis through linear model (Mathematical) for the prediction of surface roughness in turning operation.

- Rasch and Rolstadas [1971] worked on the series of finish turning tests, the surface roughness value has been observed under variation of parameters: material quality, tool quality, tool nose radius, feed, speed and cutting time. For one material and one tool quality the test results have been treated by a combined method for regression and multiple correlation analysis in order to establish that describes the surface roughness by the significant parameters.

- Taraman et al [1974] developed a mathematical model for the surface roughness in a turning operation in terms of cutting speed, feed and depth of cut. Utilizing PL1 language and an IBM 360/50 computer, the model was used to generate contours of surface roughness in planes containing the cutting speed and feed at different levels of depth of cut. The surface roughness contours were to select the machining conditions at which an increase in the rate of metal removal was achieved without sacrifices in surface finish.The surface roughness model was developed by utilizing Response Surface Methodology.

- Sundaram et al [1981] developed mathematical models to predict surface finish in fine turning of steels Part I. This paper outlines the experimental development of mathematical models for predicting the surface finish of AISI 4140 steel in fine turning operation using TiC coated tungsten carbide throw-away tools. A novel experimental design called the Rota table design was used for the experimental procedures. Variables included in the model are: cutting speed, feed, depth of cut, and time of cut of the tool. Statistical coding was used for the experimental variables. First order (log transformed) models were developed. For tools that exhibited lack of fit for the first-order models, a second-order model was developed. Multiple regression analysis was used in developing these prediction models.

- Kirby et al [1981] study in-process surface roughness prediction system, however, is an approach that can be used to indirectly determine the surface roughness of a work piece without the concern of components being negatively affected by the cutting process itself.

The surface roughness of the finish-turned work pieces was measured using a

Federal Pocket Surf stylus profilometer, set up to measure Ra in μ-inch, with a

travel length of 0.1 inch. The vibration data collection system was comprised of

an accelerometer from which signals are amplified, converted to digital data, and

processed using Windows-based software. The accelerometer sensor used was a

PCB Piezotronics #356B08 triaxial accelerometer, which was mounted on the

shank of the tool holder, directly below the cutting tool. The axes of the

accelerometer were aligned with the axes of the lathe (X, Y, and Z), using the

Applicable surfaces on the tool turret as references

- Hassan and Suliman [1990] studied a two-stage method for obtaining mach inability data for the steel turning process. In the first-stage, different mathematical model types are developed and compared for the turning process of medium carbon steel. The parameters of the models are established by curve fitting of experimental data which are collected from experiments conducted especially for this work. In the second stage, the model type(s) producing the best estimates of performance is/are used as aid in process optimization. Consequently, optimal mach inability data is obtained for maximum removal of metal. This paper aims at developing modeling tools for turning medium carbon steels (225-275 BHN) with tungsten carbide tip (Sandvik Coromant SNMG 12 04 04-15).

Mathematical programming was applied to determine optimum cutting conditions by both deterministic and probabilistic models. Also, the optimal cutting conditions were approached by a manufacturing economics-based model consisting of cost elements required for a machining operation.

- Yeo [1995] developed a methodology for an effective optimization of machining conditions of multi pass lathe operations and came to a conclusion that a single computer assisted optimization strategy that incorporates practical constraints can be used in industry W.H.Yang,

- Y.S.Tarng [1997] made a model to optimize the cutting parameters in turning operation. In this study it has been shown that tool life and surface roughness can be improved significantly for turning operation. The confirmation experiments were conducted to verify the optimal cutting parameters and there was an improvement of 250% by conducting the experiments according to optimal parameters.

- Yang and Tarng [1998] made a model to optimize the cutting parameters in turning operation. In this study it has been shown that tool life and surface roughness can be improved significantly for turning operation. The confirmation experiments were conducted to verify the optimal cutting parameters and there was an improvement of 250% by conducting the experiments according to optimal parameters.

- Malakutti and Raman [2000] developed an artificial neural network model to optimize machine setup. Here artificial neural network model was used by varying process parameters i.e. speed, feed and depth of cut to  optimize cutting force, tool life, cutting temperature and surface finish.

- Feng [2001] studied the impact of turning parameters on surface roughness. He studied the impact of Feed, Speed, and Depth of Cut, Nose radius of tool and work material on the surface roughness of work material. He found that the feed have most significant impact on the observed surface roughness and also observed that there were strong interactions among different turning parameters.

- Feng and Wang [2002] developed a model considering the following working parameters: work-piece hardness (material), feed, cutter nose radius, spindle speed and depth of cut. Two competing data mining techniques, nonlinear regression analysis and computational neural networks, are applied in developing the empirical models. The values of surface roughness predicted by these models are then compared with those from some of the representative models in the literature. Metal cutting experiments and tests of hypothesis demonstrate that the models developed in this research have a satisfactory goodness of fit. It has also presented a rigorous procedure for model validation and model comparison.

- Tugrul Ozel and Yigit Carpat [2003] used a neural network modeling approach to predict surface roughness and tool wear in turning operation. The factors considered were work piece properties ,tool material , tool geometry and cutting conditions in it a prediction system was developed which was capable of accurate surface roughness and tool wear prediction for the range it has been trainedLee and Chen [2003] have developed an online surface roughness recognition system using artificial neural network in turning operation. In their model, vibration signatures in the three directions have been used. The cutting tool with constant nose radius has been considered in their analysis.

- Chien and Tsai [2003] used the back propagation neural network for predicting the tool wear and determining the optimum cutting condition in turning operations. They used the genetic algorithm in the optimizing model as well as Taguchi method to find the optimum parameter for both the models.

- Cus and Zuperl [2003], proposed a neural network-based approach to complex optimization of cutting parameters. It describes the multi-objective technique of optimization of cutting conditions by means of the neural networks taking into consideration the technological, economic and organizational limitations. To reach higher precision of the predicted results, a neural optimization algorithm is developed and presented to ensure simple, fast and efficient optimization of all important turning parameters.

- Uros Zuperi and Francis Cus [2003] used neural networks to optimize cutting conditions and it was found that procedure is useful for the fast approx. determination of optimum cutting conditions

- Jiao et al [2004], fuzzy adaptive networks in machining process modeling to predict surface roughness in turning operation and found that feed is most significant and also came to a conclusion that this approach is more powerful than the classical regression approach.

- Sahin and Motorcu [2004], found that feed rats, nose radius, work material  and speed has significant impact on observed surface roughness but depth of cut has a little effect on the results. They also found that interactions play a significant role in the process.

- Palanikumar et al [2005] used the design of experiment concept for developing a procedure to assess and optimize the chosen factors to attain minimum surface roughness by incorporating response table and response graph, normal probability plot and ANOVA technique. Pal and Chakraborty [2005] developed a back propagation neural network model for the prediction of surface roughness in turning operation. A large number of experiments were performed on mild steel work-pieces using high speed steel as the cutting tool. Process parametric conditions including speed, feed, depth of cut, and the measured parameters such as feed and the cutting forces are used as inputs to the neural network model. Roughness of the machined surface corresponding to these conditions was the output of the neural network. The convergence of the mean square error both in training and testing came out very well

Chapter 3

REGRESSION ANALYSIS & DESIGN OF EXPERIMENT

In this chapter, regression analysis and design of experimental has been discussed for experiment design and analysis of the machining data.

3.1 Regression Analyses

Regression Analysis is a statistical forecasting model, that is concerned with describing and evaluating the relationship between a given variable (usually called the dependent variable) and one or more other variables (usually called the independent variables).

3.2 Linear Regression

In statistics, linear regression is a regression method that allows the relationship between the dependent variable Y and the p independent variables X and a random term ε. The model can be written as

Y = β1 + β2 X2 +………. + βpXp + ε

Where β1 is the intercept ("constant" term), the βI are the respective parameters of independent variables, and p is the number of parameters to be estimated in the linear regression.

This method is called "linear" because the relation of the response to the explanatory variables is assumed to be a linear function of the parameters. It is often erroneously thought that the reason the technique is called "linear regression" is that the graph of       Y = β0 + βX is a straight line or that Y is a linear function of the X variables. But if the model is (for example)

Y = α + βX + γX ²

The problem is still one of linear regression, that is, linear in x and x2 respectively, even though the graph on x by itself is not a straight line.

There are many different approaches to solving the regression problem that is, determining suitable estimates for the parameters.

3.2.2 Nonlinear Regression

In statistics, nonlinear regression is the problem of inference for a model

y = f (x, θ) + ε

Based on multidimensional x,y data, where f is some nonlinear function with respect to unknown parameters θ. At a minimum, we may like to obtain the parameter values associated with the best fitting curve (usually, least squares).Also, statistical inference may be needed, such as confidence intervals for parameters, or a test of whether of not the fitted model agrees well with the data.

The scope of nonlinear regression is clarified by considering the case of polynomial regression, which actually is best not treated as a case of nonlinear regression. When f takes a form such as

F(x) = ax2 + bx + c

Our function f is nonlinear as a function of x but it is linear as a function of unknown parameters a, b, and c. The latter is the sense of "linear" in the context of statistical regression modeling. The appropriate computational procedures for polynomial regression are procedures of (multiple) linear regression with two predictor variables x and x2 say. However, on occasion it is suggested that nonlinear regression is needed for fitting polynomials. Practical consequences of the misunderstanding include that a nonlinear optimization procedure may be used when the solution is actually available in closed form. Also, capabilities for linear regression are likely to be more comprehensive in some software than capabilities related to nonlinear regression.

3.3 Analysis Technique

3.3.1 Least-squares analysis

Least-squares analysis was developed by Carl Friedrich Gauss in the 1820s. This method uses the following Gauss-Markov assumptions:

- The random errors εi have expected value 0.

- The random errors εi are uncorrelated (this is weaker than an assumption of probabilistic independence).

- The random errors εi are homoscedastic, i.e., they all have the same variance.

These assumptions imply that least-squares estimates of the parameters are optimal in a certain sense.

A linear regression with p parameters (including the regression intercept β1) and n data points (sample size), with n >= (p + 1) allows construction of the following vectors and matrix with associated standard errors:

or, from vector-matrix notation above,

Y = Xβ + ε

Each data point can be given as , i = 1,2,3………..n. For n = p, standard errors of the parameter estimates could not be calculated. For n less than p, parameters could not be calculated.

The estimated values of the parameters can be given as

= (XTX)-1 XT

Using the assumptions provided by the Gauss-Markov Theorem, it is possible to analyze the results and determine whether or not the model determined using least-squares is valid. The number of degrees of freedom is given by m − n.

The residuals, representing 'observed' minus 'calculated' quantities, are useful to analyze the regression. They are determined from

The standard deviation,  for the model is determined from

The variance in the errors can be described using the Chi-square distribution:

The 100(1 − α) % confidence interval for the parameter, βi, is computed as follows:

where t follows the Student's t-distribution with m − n degrees of freedom and (XTX)ii -1 denotes the value located in the ith row and column of the matrix.

The 100(1 − α) % mean response confidence interval for a prediction (interpolation or extrapolation) for a value is given by:

Where,

The 100(1 − α) % predicted response confidence intervals for the data are given by:

The regression sum of squares SSR is given by:

SSR =   ∑ (i  -  ) 2

Where  is an n by 1 unit vector.

The error sum of squares ESS is given by:

ESS = ∑ (yi - i) 2

The total sum of squares TSS' is given by

TSS = ESS + SSR

Pearson's co-efficient of regression, R2 is then given as:

Assessing the least-squares model

Once the above values have been corrected, the model should be checked for 2 different things:

- Whether the assumptions of least-squares are fulfilled and

- Whether the model is valid

3.3.2 Model assumptions

The model assumptions are checked by calculating the residuals and plotting them. The residuals are calculated as follows:

The following plots can be constructed to test the validity of the assumptions:

- Plotting a normal probability plot of the residuals to test normality. The points should lie along a straight line.

- Plotting a time series plot of the residuals, that is, plotting the residuals as a function of time.

- Plotting the residuals as a function of the explanatory variables, X.

- Plotting the residuals against the fitted values,.

- Plotting the residuals against the previous residual.

In all, but the first case, there should not be any noticeable pattern to the data.

3.3.3 Model validity

The validity of the model can be checked using any of the following methods:

- Using the confidence interval for each of the parameters, βi. If the confidence interval includes 0, then the parameter can be removed from the model. Ideally, a new regression analysis excluding that parameter would need to be performed and continued until there are no more parameters to remove.

- Calculate Pearson’s co-efficient of regression. The closer the value is to 1; the better the regression is. This co-efficient gives what fraction of the observed behavior can be explained by the given variables.

- Examining the observational and prediction confidence intervals. The smaller they are the better.

- Computing the F-statistic.

Confidence or prediction interval of a regression line

If you check the option box, Prism will calculate and graph either the 95% confidence interval or 95% prediction interval of the regression line.  Two curves surrounding the best-fit line define the confidence interval.

Fig. 3.1

The dashed lines that demarcate the confidence interval are curved. This does not mean that the confidence interval includes the possibility of curves as well as straight lines. Rather, the curved lines are the boundaries of all possible straight lines. The fig. below shows four possible linear regression lines (solid) that lie within the confidence interval (dashed).

Fig. 3.2

Given the assumptions of linear regression, you can be 95% confident that the two curved confidence bands enclose the true best-fit linear regression line, leaving a 5% chance that the true line is outside those boundaries.

Many data points will be outside the 95% confidence interval boundary. The confidence interval is 95% sure to contain the best-fit regression line. This is not the same as saying it will contain 95% of the data points.

The 95% prediction interval is the area in which you expect 95% of all data points to fall. In contrast, the 95% confidence interval is the area that has a 95% chance of containing the true regression line. This graph shows both prediction and confidence intervals (the curves defining the prediction intervals are further from the regression line).

Fig. 3.3

The analysis of Experimental results obtained of surface roughness was analyzed. The data for speed, feed, depth of cut and surface roughness was recorded and analyzed in terms of obtaining best fit curve equations.

3.4 Parameter Design Optimization of CNC Turning Using DOE

This chapter is all about the steps and procedures used to optimize turning parameters using Taguchi’s design of experiment. In this chapter objectives of the study were set and according to the objectives of the study different factors were selected. After that experimental work was carried out on CNC turning machine according to L27 orthogonal array. The values of response factor i.e. surface roughness are then recorded according to orthogonal array.

##### 3.4.1 Concept of DOE

Design of Experiment (DOE) is a structured, organized method that is used to determine the relationship between the different factors (Xs) affecting a process and the output of that process (Y). Sir Ronald A. Fisher, the renowned mathematician and geneticist first developed this method in the 1920s and 1930.

Design of experiment (DOE) is to understand the impact of specific changes to the inputs of the process, and then to maximize, minimize or normalize the outcome by manipulating the input.

DOE is a scientific approach which allows the researchers to gain knowledge in order to better understand a process and to determine how the impacts (attribute effect the output response).

It is usually used when it is unclear what impact a specific set of inputs may have either individually or collectively on process or product. A designed experiment is the simultaneous evaluation of two or more factors (parameters) for their ability to affect the resultant average or variability of a particular product or process characteristic. To accomplish this in an effective and statically proper fashion, the level of factors are varied in a strategic manner, the results of particular test combination are observed, and the complete set of results is analyzed to determine the influential factors and preferred levels, and whether increase or decrease of those levels will potentially lead to further improvement. It is important to note that this is an iterative process; the first round through the DOE process will many times lead to subsequent rounds of experimentation. The beginning round, often referred to as screenings experiment, is used to find the few important influential factors out of the many possible factors involved with the process or product design. The experiment is typically a small experiment with many factors at two levels. Later rounds of experiments typically involve few factors at more than two levels to determine conditions of further improvement.

- DOE is the most cost effective and efficient method for identifying the key input factors and in understanding the relationship between input factors and response.

- DOE investigate a number of input factors with relatively small number of tests.

- DOE helps to identify important/ critical attributes of a process improvement effort, as they can be characteristics to be examined and the desired effect.

The DOE process is divided is divided into three main phases, which encompasses all experimental approaches. These three phases are:

  - The Planning Phase

  - The Conducting Phase

  - The analyzing phase.

The planning phase is when factors and levels are selected and, therefore the most important stage of experimentation. Also the correct selection factors and levels is non statistical in nature and more dependent upon product or process expertise.

The second most important phase is the conducting phase, when the test results are actually collected. If experiments are well planned and conducted, the analysis is actually much easier and more likely to yield positive information about factors and levels.

The analysis phase is when the positive or negative information concerning the selected factors and levels is generated based on the previous two phases. This phase is statistical in nature.

The major steps to complete an effective designed experiment are listed in the following 12 steps. The planning phase includes steps 1 through 9, the conducting step 10, and the analysis phase include steps 11 and 12.

- State the problem(s) or areas(s) of concern.

- State the objective(s) of the experiment.

- State the quality characteristic(s) and measurement system(s).

- Select the factors that may influence the selected quality characteristics.

- Identify control and noise factors.

- Select levels of factor.

- Select the appropriate orthogonal array (OA) or Ors.

- Select interactions that may influence the selected quality characteristics or go back to step 4(iterative steps).

- Assign factors to OA(s) and locate interactions.

- Conduct tests described by trials in OAs.

- Analyze and interpret results of the experimental trials.

- Conduct confirmation experiment.

3.4.2 Problem Identification

Set-up parameters play the most important role to get the desired results. The main objectives of this research are to carry out the experiments by selecting different variables and their levels, applying Taguchi design of experiment and then analyzing the results obtained. Quality characteristics considered is:

- Surface Roughness

The set-up parameters, which were used to get the expected results, are

- Spindle Speed

- Feed

- Depth of Cut

- Nose radius

The experiments were conducted according to the Taguchi design of experiment i.e. the number of experiments were done as suggested by the Taguchi design of experiment according to number of factors, their levels and their interactions.

3.4.3 Taguchi's Parameter Design Method

3.4.3.1 Objective of Taguchi's Method

Taguchi's parameter design can be used to make a process robust against sources of variation and hence improve field performance. If we can design a process that has the robustness to noise factors that largely affects the variance of performance characteristics at a developing stage, it will very possible for the process to have robustness against other noise factors that could not be considered at the development stage. The aim of a parameter design experiment is, then, to identify settings of the design parameters that maximize the chosen performance measure and are insensitive to noise factors.  (Feng. Chang-Xue (Jack) 2001)

3.4.3.2 Orthogonal Array

The goal of a Taguchi's experimental design is to identify optimal settings for all the design parameter, not to build the model fitting of process. Taguchi has achieved substantial payoffs just by conducting many main-effect-only-experiments and checking the results by confirmation experiments. If it can be proved that the system could be described well by even only main effects, the optimal condition determined by only main effect analysis can be very efficient and simple method for optimization. Orthogonal array has been used to minimize the number of test runs while keeping the pair-wise balancing property in Taguchi's method for that purpose. These basic principles serve as a screening filter, which allows the examination of the effects of many process variables, identifying those factors, which have a major effect on process characteristics using a single trial with a few reactions. For example, optimization experiment would normally require each variable to be tested independently. Thus, a trial run investigating the effects and interactions of four reaction variables each at three concentration levels, would require an experiment with 81 (i.e. 34) separate reactions. Using an orthogonal array, however, an estimate of the effect of each variable can be carried out using only nine experiments. Providing that three level are used for each variable tested, the number of experiments required (E) is calculated from the equation E= 2k +1, where k is the number of factors to be tested. If the calculated number is not a multiple of three, then the required number of variables to be tested is the next multiple. Hence, as the number of components to be tested is increased, the reduction in the number of experiments required becomes more marked; e.g. to test 9 factors would require 39 = 19683 experiments to analyze fully, whereas using Taguchi's methods this could be reduced to just 21(2 x 9 + 1 = 19), 19 is not a multiple of three and then next integer divisible by three is 21).

3.4.4 Brainstorming

When physical experiments are used, it is sometimes impossible or very expensive to carry out an experiment according to the set-up. Thus it becomes necessary to first study and discuss about the process and process parameters. A good knowledge about the work to be done, process and optimization technique may be very helpful to get expected results. Important steps that are to be considered are as follows:

- Objectives of Study and Evaluation Criteria

- What are the criteria of evaluation?

- How are each of these criteria measured?

- How are these criteria combined into a single number?

- What is the common characteristic of these criteria?

- What is the relative influence these criteria exhibit?

- Design Factors

- What are the factors that influence the performance criteria?

- Which factors are more important than others?

- Noise Factors

- Which factors can't be controlled in real life?

- Is the performance dependent on the application environment?

- Factor Levels

- What are the ranges of values the factors can assume within  practical limits?

- How many levels of each factor should be used for the study?

- What is the tradeoff for a higher level?

- Interaction between Factors

- Which factors are most likely to interact?

- How many interactions can be studied?

- Scopes of Studies

- How many experiments can we run?

- When do we need the results?

- How much does each experiment cost?

- Additional Items

- What do we do with factors that are not included in the study?

- In what order do we run these experiments?

- Who will do these experiments?

Use of Orthogonal Arrays (OAs) and Signal-to-Noise (S/N) Ratios

OAs is used to minimize the number of runs (or combinations) needed for the experiment. Many people are of the opinion that the application of OA is TM, but the application of OAs is only a part of TM. S/N ratios are used as a measure of the functionality of the system. S/N ratios capture the magnitude of real effects (signals) after making some adjustment to uncontrollable variation (noise).

Two-Step Optimization

After conducting the experiment, the factor–level combination for the optimal design is selected with the help of two step optimization. The first step is to minimize the variability (maximize S/N ratios). In the second step, the sensitivity (mean) is adjusted to the desired level since it is easier to adjust the mean after minimizing the variability.

3.4.5 Types of Optimization Problems

3.4.5.1 Static Problems

Generally, a process to be optimized has several control factors, which directly decide the target or desired value of the output. The optimization then involves determining the best control factor levels so that the output is at the target value. Such a problem is called as a "STATIC PROBLEM".

This is best explained using a P-Diagram, which is shown below ("P" stands for Process or Product). Noise is shown to be present in the process but should have no effect on the output. The primary aim of the Taguchi experiments is to minimize variations in output even though noise is present in the process. The process is then said to have become robust.

Fig. 3.4 P-Diagram for Static Problems

3.4.5.2 Dynamic Problems

If the product to be optimized has a signal input that directly decides the output, the optimization involves determining the best control factor levels so that the "input signal / output" ratio is closest to the desired relationship. Such a problem is called as a "DYNAMIC PROBLEM". The difference between dynamic and static problem is that in dynamic problems we study the effects on output due to noise also which are not considered in static problems. This is best explained by a P-Diagram, which is shown below. Again, the primary aim of the Taguchi experiments - to minimize variations in output even though noise is present in the process- is achieved by getting improved linearity in the input/output relationship.

Fig. 3.5 P-Diagram for Dynamic Problems

3.4.6 Batch Process Optimization

There are 3 Signal-to-Noise ratios of common interest for the purpose of optimization;

3.4.6.1 Smaller-The-Better 
n = -10 Log10 [mean of sum of squares of measured data]

This is usually the chosen S/N ratio for all undesirable characteristics like "defects, surface roughness" etc. for which the ideal value is zero. Also, when an ideal value is finite and its maximum or minimum value is defined (like maximum purity is 100% or minimum time for making a telephone connection is 1 sec) then the difference between measured data and ideal value is expected to be as small as possible. The generic form of S/N ratio then becomes,

n = -10 Log10 [mean of sum of squares of {measured - ideal}]

3.4.6.2 Larger-The-Better

n = -10 Log10 [mean of sum squares of reciprocal of measured data]

This case has been converted to SMALLER-THE-BETTER by taking the reciprocals of measured data and then taking the S/N ratio as in the smaller-the-better case. 
3.4.6.3 Nominal-The-Best

Square of mean 
    n = 10 Log10      ----------------- 
                                variance

This case arises when a specified value is MOST desired, meaning that neither a smaller nor a larger value is desirable.

3.4.7 Steps in Taguchi Methodology

Taguchi method is a scientifically disciplined mechanism for evaluating and implementing improvements in products, processes, materials, equipment, and facilities. These improvements are aimed at improving the desired characteristics and simultaneously reducing the number of defects by studying the key variables controlling the process and optimizing the procedures or design to yield the best results.

The method is applicable over a wide range of engineering [35] fields that include processes that manufacture raw materials, sub systems, products for professional and consumer markets. In fact, the method can be applied to any process be it engineering fabrication, computer-aided-design, banking and service sectors etc. Taguchi method is useful for 'tuning' a given process for 'best' results.

Taguchi proposed a standard 8-step procedure for applying his method for optimizing any process. These are:

Step1: formulation of the problem – the success of any experiment is dependent	on a full understanding of the nature of the problem. It is important to establish just what the experiment is aiming to solve.

Step2: Determine the objective:-Identify the output characteristics (responses) to be studied and eventually optimized and determine the method of measurement. To establish measurement reliability, a separate experiment may be required

Step 3: Identification of control factors, noise factors and signal factors (if any). Control factors are those which can be controlled under normal production conditions. Noise factors are those which   are either too difficult or too expensive to control under normal production conditions. Signal factors are those which affect the mean performance of the process. Taguchi believes that it is generally preferable to consider as many factors (rather than many interactions) as it is economically feasible for the initial screening.

Step 4: selection of factor levels, possible interactions and the degrees of freedom associated with each factor and the interaction effects. Assign the controllable factors and their interactions to the columns of the inner array, and the noise factors to the columns f the outer array.

Step 5: Conduct the experiment: Perform the experimental trials and collect the experimental data.

Step 6: Analyze the data: Evaluate the performance measures (TPM and NPM) for each trial run of the inner array and analyze them using the appropriate statistical analysis technique

Step 7: Interpret the results: Identify the variability control factors (VCF) and target control factors (TCF) and select their optimal levels. For the VCF’s the optimal levels are those, which maximize the NPM (minimize variability in the response), and for the TCF’s they are those, which bring the mean response nearest to the target value.

Step 8: Run a confirmatory Experiment: It is necessary to confirm, by some follow up experimental trials. A successful confirmation can alleviate concerns about the possibilities of a wrong choice for factor levels and experimental design.

If predicted results are not confirmed, or otherwise unsatisfactory, additional experiments may be required and a repetition of step no. 3 to 8 may be necessary.

3.4.8 Advantages of Taguchi Design of Experiment

- It changes the timing of the application of quality control from on line to offline, so that we can easily rely on inspection, can build quality into the product and the process and thus ‘do it right first time’.

- It changes the experiment procedure from varying one factor at a time to varying many factors at a time, through statistical experimental design techniques.

- It changes the objective of experiments and the definition of quality from ‘achieving conformance to specification’ to ‘achieving the target and minimizing the variability’.

- It changes the attitude for dealing with uncontrollable factors: remove the effect not the cause, by appropriately turning the controllable factors.

3.4.9 Limitations of Taguchi Design of Experiment

Sometimes it is claimed that, Dr. Taguchi, “has advocated some novel methods of statistical analysis and some approaches to the design of experiments that are unnecessarily complicated, inefficient, and sometimes ineffective”.

- Some of Taguchi’s experiment designs may lead to an incorrect answer when large two factor interactions appear.

- Taguchi method uses one array for control variables and one array for the noise variables and then a crossed array experiment is conducted, this makes the process difficult to understand.

- Several considerations favour the separate analysis of mean value and standard deviation instead of using Taguchi’s S/N ratio.

- There is only selected number of experiments to be done in Taguchi’s design of experiment that’s why it cannot be guaranteed that picking optimum level will provide optimum results.

- This process is limited to a certain number of designs.

- It will be useful only when it is implemented in early stages of design.

Chapter 4

EXPERIMENT SET UP

In this chapter, we would discuss the experimental set up, machine used its limitations, advantages, measuring instrument, tooling used on the machine.

4.1 CNC lathe

The CNC Lathe Machine consists of the machine unit with a three jaw independent chuck, a computer numerically controlled tool slide, which cud move accordingly to two axis horizontal and vertical- X and Z axis. X axis represents the vertical movement which gives the depth of cut where as Z axis represents the location of the cutting tool. Thus after deciding the machining zero at a certain point the command is given in the form of a part program. The machine is also provided with an automatic lubrication motor for its slides.

Fig.: 3.1 CNC LATHE

Fig. 3.2 Tool holder				Fig.: 3.3 Job Piece

CNC Lathe Machine made JYOTI Rajkot GUJRAT was available for turning for ferrous and y Non-ferrous materials. The chuck holding the work piece diameter was only limited to 100 mm and the maximum work piece length was limited to about 1000 mm length

System configuration

JYOTI Rajkot Gujrat make CNC lathe is the Computer Numerically Controlled Lathe machine. This machine has following configurations.

- Machine Controller consists of :

  - Pentium IV (866 MHz) with preinstalled Windows-98

  - 128 MB RAM

  - 40 GB HDD

  - SVGA Color Monitor

  - Keyboard & Mouse

  - I/O interface card. (Inside PC)

- Electronic Stabilizer :

  - Capacity – 3KVA

  - Regulation 1%

  - Voltage 230V

  - Current – 10 Amp.

  - Frequency – 50 Hz.

- Lubrication motor :

  - Voltage – 230V

  - Current – 1 Amp.

  - Operating Pressure : 6 – 15 Kg/Cm2

- X & Z Axes Stepper motor :

  - Capacity – 13 Kg-Cm for X Axis & 20 Kg-Cm for Z Axis.

  - Operating Voltage 36V DC

  - O/P Current– 4 Amp.

- Power supply :

  - Input 230V, 5 Amps.

  - Output 24V, 2 Amps.

  - 5V, 2 Amp, 15/0/ - 15V 500 mA

- SPECIFICATIONS OF I/0 CARD: (PCI 1751) :

  - I/O Controller – 8255-2

  - Slot for connection – PCI slot on the motherboard of the PC.

  - I/O Lines – 32 output & 16 inputs.

Table 4.1 CNC lathe Machine specifications

| Model | DX-250 |
| --- | --- |
| Swing over bed | 250mm |
| Swing over cross slide | 100mm |
| Distance between centers | 400mm |
| Max. Longitudinal Travel | 350mm |
| Spindle inside diameter | MT3 |
| Type of bearing for spindle | Angular contact bearings |
| Spindle Speed | 50 to 25000 rpm |
| Thrust (max.) | 120 kg |
| Cross Slide inclination | 0 deg. |
| Standard cutting tool size | 16*16mm |
| Spindle Motor | 12/15 kw |
| Threading | Straight |
| Automatic Lubrication points | Provided |
| Input System | Metric/inch |
| Control Axes | Simultaneous |
| Interpolation | Linear and circular |
| Minimum movement command X | 0.005 |
| Minimum movement command Z | 0.005 |
| Rapid Feed Rate X | 200 mm/min |
| Rapid Feed Rate X | 400 mm/min |
| X axis ballscrew | 16mm* 5mm PITCH |
| Z axis ballscrew | 25mm* 5mm PITCH |
| Feed override | 100% |
| Dwell (sec) | Programmable |
| Backlash compensation | Provided |
| Constant surface speed control | G96, G97 |
| Canned Cycles | Available |
| In Built interface | Serial, Parallel |
| Manual reference point return | Provided |
| Emergency Stop | Provided |
| S function | Provided |
| Floor Space required | 1100* 700mm |
| Overall height of machine | 1450 mm |
| Net weight | 5700 kg |

4.2 Surface Roughness Measuring Instrument

The Surtronic 3+ is a portable, self-contained instrument for the measurement of surface texture and is suitable for use in both the workshop and laboratory. Parameters available for surface texture evaluation are: Ra, Rq, Rz, Ry, Rt and Sm.

The parameters evaluations and other functions of the instrument are microprocessor based. The measurement results are displaced on an LCD screen and can be output to an optional printer or another computer for further results.

The instrument is normally powered by an alkaline non-rechargeable battery. If preferred, a Ni-Cad rechargeable battery can be used.

Fig.: 4.2 Surface roughness measurement apparatus (Referred from Instrument Manual)

Display-Transverse Unit

The top panel of the display-traverse unit carries a membrane type control panel and a liquid crystal display. The unit houses the electronics for controlling the measurement sequence, computing the measurement data and outputting the results to the display, or to the RS232 port for use with a printer( when included) or to a computer for further analysis.

The unit also contains a drive motor which traverses the pickup across the surface to be measured. The measuring stroke always starts from the extreme outward positions. At the end of the measurement the pick up returns to this position ready for the next measurement. The traverse length is determined from selections of cut-off (Lc) or length (Ln).

Fig.: 4.3 Display Transverse Unit (Referred from Instrument Manual)

Pick-Up Mounting Components

The pick-up is fastened to the drive shaft by the following means:

Mounting Bracket:  This is clamped to the drive shaft by means of a knurled knob. Although normally used upright, it can be turned to angle the pick-up or to take it off the centre line. It can also be mounted sideways on the drive shaft, when the right-angle pick-up is in use.

Fig.: 4.4 Mounting Bracket (Referred from Instrument Manual)

Adjustable Support: this can be clamped at any positions on the slide of the mounting bracket to provide pick-up height adjustment.

Pick-up Holder: This fits into the crutch of the pick-up support and is held in place by a spring plunger.

Connector: the connector of the pick-up lead is screwed into the end of pick-up and is then inserted into the end of the pick-up holder, with the lead coming out through the slot in the holder. It is advisable to connect the lead to the display-traverse unit first and then to the pick-up. When the extension rod is used, the short pick-up is not required and the end of the rod itself is inserted into the holder.

DIP switch settings: The instrument default settings, when powering up with a new battery, are set via DIP switches housed inside the display-traverse unit. The selections can be changed by menu/pushbuttons operations. The DIP switches are accessed by unscrewing the three feet from the base of the display-traverse unit, then removing the screws which were partly covered by the feet.

Pick-up

The pickup is a variable reluctance type transducer which is supported on the surface to be measured by a skid, a curved support projecting from the underside of the pickup in the vicinity of the stylus. As the pickup traverses across the surface, movements of the stylus relative to the skid are detected and are converted into a proportional electrical signal. The radius of curvature of the skid is much greater than the roughness spacing. This enables it to ride across the surface almost unaffected by the roughness, and provides a datum representing the general form of the surface. Even so, where the waviness is widely spaced it will be necessary to use the pickup with shoe, in conjunction with the 2.5mm (0.1 in) cut-off.

Fig.: 4.5 Pick-up (Referred from Instrument Manual)

Specifications of Roughness Measurement Instrument:

Make   :			Taylor/Hobson (Supplied from England)

Battery:	Alkaline: Minimum 600 Measurements of 4mm Measurements Lengths.

Ni-Cad: Minimum 200 Measurement of 4mm Length

Size: 6 LR 61 (USA/Japan), Fixed Battery

External Charger (Ni-Cad Only)

110/240V, 50/60 Hz

Traverse Unit:		Traverse Speed: 1mm/Sec

Measurement:		Metric/Inch Preset by DIP-Switch

Cut-Off Values: 		0.25mm, 0.8mm, and 2.50mm

Traverse Length: 	1, 3, 5, 10, Or 25.4 + 0.2mm At 0.8mm Cut-Off.

Display: 		LCD-Matrix. 2lines * 16 Characters

Keyboard:		Membrane Switch Panel Tactile.

Filters:	Digital Gauss Filters or 2CR Filter (ISO) Selectable By DIP-Switch.

Parameters:		Ra, Rq, Rz (DIN), Ry and Sm.

Calculations Time: 	Less Than Reversal Time Or 2 Sec Which Ever Is The Longer.

4.3 Work piece material.

Standardized material was selected to ensure consistency of the alloy, which is an EN8 used in industry thus, EN8 made in the form of bars with the varying size of diameter (in steps) so as to fit under the chuck. To more closely replicate typical finish turning processes and to avoid excessive vibrations due to work piece dimensional inaccuracies and defects, each work piece was rough-cut just prior to the measured finish cut.

After one rough cut on each work piece so as to smooth the surface, we divide each work piece into three zones with length starting from one face from where tool starts cutting. Thus simultaneously we could choose the machining zero required for generating cutting profile with reference to our work piece dimensions. These three zones of machining would represent three different values of feed at one depth of cut and at a single speed. These zones were from 0-25 mm, 25-50 mm and 50-75 mm from the machining zero side. Surtronic 3+ instrument available has a pickup with a skid which is used to travel automatically through a drive motor. Thus such travel would at least require a distance of at least 20 mm. Thus we require appropriate surface travel distance on turned gun metal work piece. These dimensions were taken so as to keep travel the stylus on the best surface as the cutting could improper at the starting or at the end. In this way the error in measurement could also be reduced and there are less chance of measuring the wrong side values.

4.4 Cutting Tool Material

The cutting tool which is provided with the CNC lathe Machine was a 30 mm square tool with 60 mm Length having the same tool angles as for a normal turning tool. The basic properties of CARBIDE tools are Superior hot hardness and wear resistance. These can retain hardness at temperatures above 600C but soften rapidly at higher temperatures. Cutting Speeds are limited upto 0.75 to 1.8 m/sec.

The tool used was cemented carbide insert type. The geometry of tool is: Rake angle 60 (+ve), 50 (+ve) clearance angle, 600 (+ve) major cutting edge angle, 600 (+ve) included angle and 00 cutting edge inclination angle. The work piece material was EN8 alloy with the chemical composition as under:

TABLE 4.2 (Chemical Composition of Work Piece)

| Element | Weight % |
| --- | --- |
| C. | 0.40% |
| Si | 0.25% |
| Mn | 0.80% |
| S | 0.05% max |
| P | 0.05% max |

EN8 in US equivalent is to AISI - C 1038/ C1041

Mechanical properties - normalized /hardened and tempered

Limiting Ruling Section (in) - 6 /2 1/2

Tensile Strength (tons/sq.in) - 35 (min) /40 (min)

Yield Strength (tons/sq.in.) - 18 (min) /28 (min)

Elongation % - 20 /22

Izod Impact Value (Ft.Lb) - 25 (min)

Weld ability POOR

Application - Medium strength material used for nuts, for high tensile studs and for rotor

Forgings. Obtainable in various grades A, B, C, D, and E according to properties required

- 4.5 Measurement of Surface Roughness

Inspection and assessment of surface roughness of machined work pieces can be carried out by means of different measurement techniques. These methods can be ranked into the following classes:

- Direct measurement methods

- Comparison based techniques

- Non contact methods

- 4.5.1 Direct Measurement Methods

Direct methods access surface finish by means of stylus type devices. Measurements are obtained using a stylus drawn along the surface to be measured. The stylus motion perpendicular to the surface is registered. This registered profile is then used to calculate the roughness parameters. The parameter Ra is used here.

Fig. 4.6 (Measurement of Surface roughness by Stylus)

- 4.5.2 Comparison Based Techniques

Comparison techniques use specimens of surface roughness produced by the same process, material and machining parameters as the surface to be compared. Visual and tactile senses are used to compare a specimen with a surface of known surface finish. This method is useful for surface roughness Ra>1.6 micron.

- 4.5.3 Non Contact Methods

- In it a rough surface is illuminated by a monochromatic plane wave with an angle of incidence with respect to the normal to the surface.  The photo sensor of a camera placed in the focal plane of a Fourier lens is used for recording speckle patterns. Then the surface roughness can be defined and calculated

In these experiments direct measurement method has been used i.e. stylus type surface roughness meter was used to measure the surface roughness of the specimen. There were two main reasons behind selecting stylus type surface roughness; one is its easy availability and other is the ease with which it can be operated. The instrument used in these experiments is a product of precision devices.

4.6 Factors and their Levels

The factors and their levels have been selected on the basis of tool, work piece material, machine parameters and by studying different research papers and data hand books. Different cutting parameters and their level are shown in table:

Table 3.3 Process Parameters

| Process parameters | Levels |  |  |
| --- | --- | --- | --- |
| R.P.M. | 400 | 600 | 800 |
| Depth of Cut (mm) | 0.7 | 1.6 | 2.0 |
| Feed (mm/rev.) | 0.1 | 0.2 | 0.3 |
| Nose Radius (mm) | 0.4 | 0.8 | 1.2 |

Chapter 5

ANALYSIS OF MACHINING DATA

Regression analysis is one of the most widely used techniques for analyzing multifactor data. Its broad appeal and usefulness result from the conceptually logical process of using an equation to express the relationship between a variable of interest (the response) and a set of related predictor variables. So regression analysis was used to develop the parametric equations. The following factors are used in the present analysis:

Regression sum of squares:

SSR=i=1nyi−y2								(5.1)

Where y= sum of dependent variable

yi= fitted value of ith dependent variable

Residual sum of squares:

SSRes=i=1nyi−yi2								(5.2)

yi = observed value of ith dependent variable

Total sum of squares: It is the total variability in the observations of the data.

SST=SSR+SSRes								(5.3)

Predictor variables

k=SSR  σ2									(5.4)

This has the same number of degree of freedom as number of regressor or predictor variables in the model.

σ2 = variance

Regression mean squares

MSR=SSRk									(5.5)

Residual mean squares

MSRes=SSResn−p								(5.6)

p = k +1 = parameter in the regression model

n = number of observations

Test of statistic

F=MSRMSRes									(5.7)

Coefficient of determination

R2=SSRSST=1−SSResSST							(5.8)

Adjusted coefficient of determination

Adjusted R2=1−SSResn−pSSTn−1						(5.9)

Standard error of regression:	SE=MSRes			          (5.10)

5.1 Mathematical Models Formulation of Machining Data

The purpose of developing the mathematical models relating the machining responses and their machining factors was to facilitate the optimization of the machining process. Using these mathematical models, the objective function and process constraints were formulated, and the optimization problem was then solved by using regression analysis.

The mathematical models commonly used are represented by:

Y=φV,f,d, NR         								(5.11)

Where Y is the machining response,

ϕ is the response function,

and V, f, d, NR are machining variables.

5.1.1 Non-Linear Model

When expressed in the non- linear form, equation 5.11 becomes

Y=C Vn1 fn2 dn3 NRn4								(5.12)

The surface roughness model was formulated as:

Ra=C Vn1 fn2 dn3 NRn4							(5.13)

Logarithms taken on both sides of the equation 5.13

logRa=logC+n1 log V+n2 log f+n3 log d+n4 log NR		(5.14)

Using these mathematical models, the objective function and process constraints were formulated, and the optimization problem was then solved by using regression analysis as shown in Fig. 5.1.

Surface

Roughness

Cutting speed

Feed

Depth of cut

Logarithmic transformation

Data set

Procedure

Output

Raw mach inability data

Fig. 5.1 Flow Chart for processing Non-Linear Model in regression analysis

[Yeo et al, 1989].

Table 5.1   Data Collection for Model

| Diameter (mm) | RPM | Speed (m/min) | Feed (mm/rev) | Depth (mm) | Nose Radius (mm) | Ra (μm) |
| --- | --- | --- | --- | --- | --- | --- |
| 31.06 | 400 | 39.04 | 0.2 | 0.7 | 0.4 | 4.3 |
| 33.03 | 600 | 62.27 | 0.2 | 0.7 | 0.4 | 6.16 |
| 35.11 | 800 | 88.25 | 0.2 | 0.7 | 0.4 | 4.86 |
| 37.1 | 400 | 46.63 | 0.1 | 0.7 | 0.4 | 3.72 |
| 39.05 | 600 | 73.62 | 0.1 | 0.7 | 0.4 | 4.04 |
| 40.97 | 800 | 102.98 | 0.1 | 0.7 | 0.4 | 3.86 |
| 43 | 400 | 54.04 | 0.3 | 0.7 | 0.4 | 9.02 |
| 45.05 | 600 | 84.93 | 0.3 | 0.7 | 0.4 | 6.44 |
| 47.03 | 800 | 118.21 | 0.3 | 0.7 | 0.4 | 6.02 |
| 30.92 | 400 | 38.86 | 0.2 | 1.6 | 0.4 | 4.82 |
| 32.85 | 600 | 61.93 | 0.2 | 1.6 | 0.4 | 3.2 |
| 34.83 | 800 | 87.55 | 0.2 | 1.6 | 0.4 | 3.1 |
| 36.79 | 400 | 46.24 | 0.1 | 1.6 | 0.4 | 2.58 |
| 38.77 | 600 | 73.09 | 0.1 | 1.6 | 0.4 | 2.02 |
| 40.75 | 800 | 102.43 | 0.1 | 1.6 | 0.4 | 1.28 |
| 42.85 | 400 | 53.85 | 0.3 | 1.6 | 0.4 | 7.12 |
| 44.76 | 600 | 84.38 | 0.3 | 1.6 | 0.4 | 6.36 |
| 46.74 | 800 | 117.49 | 0.3 | 1.6 | 0.4 | 6.36 |
| 30.93 | 400 | 38.87 | 0.2 | 2 | 0.4 | 4.8 |
| 32.88 | 600 | 61.99 | 0.2 | 2 | 0.4 | 3.7 |
| 34.87 | 800 | 87.65 | 0.2 | 2 | 0.4 | 3.38 |
| 36.81 | 400 | 46.26 | 0.1 | 2 | 0.4 | 2.38 |
| 38.82 | 600 | 73.18 | 0.1 | 2 | 0.4 | 1.66 |
| 40.79 | 800 | 102.53 | 0.1 | 2 | 0.4 | 1.16 |
| 42.83 | 400 | 53.83 | 0.3 | 2 | 0.4 | 7.86 |
| 44.83 | 600 | 84.51 | 0.3 | 2 | 0.4 | 6.66 |
| 46.78 | 800 | 117.59 | 0.3 | 2 | 0.4 | 7.1 |
| 31.8 | 400 | 39.97 | 0.2 | 0.7 | 0.8 | 5.78 |
| 32.99 | 600 | 62.19 | 0.2 | 0.7 | 0.8 | 5.06 |
| 34.95 | 800 | 87.85 | 0.2 | 0.7 | 0.8 | 2.04 |
| 36.9 | 400 | 46.38 | 0.1 | 0.7 | 0.8 | 4.82 |
| 38.89 | 600 | 73.32 | 0.1 | 0.7 | 0.8 | 4.34 |
| 40.9 | 800 | 102.81 | 0.1 | 0.7 | 0.8 | 2.68 |
| 42.89 | 400 | 53.90 | 0.3 | 0.7 | 0.8 | 6.92 |
| 44.9 | 600 | 84.65 | 0.3 | 0.7 | 0.8 | 3.4 |
| 46.88 | 800 | 117.84 | 0.3 | 0.7 | 0.8 | 2.68 |
| 31 | 400 | 38.96 | 0.2 | 1.6 | 0.8 | 5.66 |
| 32.98 | 600 | 62.17 | 0.2 | 1.6 | 0.8 | 3.14 |
| 34.97 | 800 | 87.90 | 0.2 | 1.6 | 0.8 | 1.54 |
| 36.98 | 400 | 46.48 | 0.1 | 1.6 | 0.8 | 3.52 |
| 38.89 | 600 | 73.32 | 0.1 | 1.6 | 0.8 | 2.56 |
| 40.89 | 800 | 102.78 | 0.1 | 1.6 | 0.8 | 1.88 |
| 42.99 | 400 | 54.03 | 0.3 | 1.6 | 0.8 | 3.06 |
| 44.89 | 600 | 84.63 | 0.3 | 1.6 | 0.8 | 1.4 |
| Diameter (mm) | RPM | Speed (m/min) | Feed (mm/rev) | Depth (mm) | Nose Radius (mm) | Ra (μm) |
| 46.87 | 800 | 117.81 | 0.3 | 1.6 | 0.8 | 2.58 |
| 31 | 400 | 38.96 | 0.2 | 2 | 1.2 | 3.02 |
| 32.92 | 600 | 62.06 | 0.2 | 2 | 1.2 | 1.38 |
| 34.89 | 800 | 87.70 | 0.2 | 2 | 1.2 | 1.76 |
| 36.87 | 400 | 46.34 | 0.1 | 2 | 1.2 | 3.02 |
| 38.83 | 600 | 73.20 | 0.1 | 2 | 1.2 | 2.5 |
| 40.81 | 800 | 102.58 | 0.1 | 2 | 1.2 | 1.24 |
| 42.82 | 400 | 53.82 | 0.3 | 2 | 1.2 | 2.5 |
| 44.85 | 600 | 84.55 | 0.3 | 2 | 1.2 | 1.56 |
| 46.84 | 800 | 117.74 | 0.3 | 2 | 1.2 | 1.54 |
| 31.02 | 400 | 38.99 | 0.2 | 0.7 | 1.2 | 4.96 |
| 32.97 | 600 | 62.16 | 0.2 | 0.7 | 1.2 | 6.82 |
| 34.99 | 800 | 87.95 | 0.2 | 0.7 | 1.2 | 5.5 |
| 36.95 | 400 | 46.44 | 0.1 | 0.7 | 1.2 | 5.24 |
| 38.9 | 600 | 73.33 | 0.1 | 0.7 | 1.2 | 2.94 |
| 40.91 | 800 | 102.83 | 0.1 | 0.7 | 1.2 | 3.96 |
| 42.09 | 400 | 52.90 | 0.3 | 0.7 | 1.2 | 52.4 |
| 44.92 | 600 | 84.68 | 0.3 | 0.7 | 1.2 | 4.62 |
| 46.91 | 800 | 117.91 | 0.3 | 0.7 | 1.2 | 3.6 |
| 31.07 | 400 | 39.05 | 0.2 | 1.6 | 1.2 | 6.46 |
| 33.35 | 600 | 62.87 | 0.2 | 1.6 | 1.2 | 5.04 |
| 35.01 | 800 | 88.00 | 0.2 | 1.6 | 1.2 | 4.82 |
| 36.96 | 400 | 46.45 | 0.1 | 1.6 | 1.2 | 4.5 |
| 38.94 | 600 | 73.41 | 0.1 | 1.6 | 1.2 | 5.22 |
| 40.93 | 800 | 102.88 | 0.1 | 1.6 | 1.2 | 3.3 |
| 42.93 | 400 | 53.95 | 0.3 | 1.6 | 1.2 | 5.9 |
| 42.92 | 600 | 80.91 | 0.3 | 1.6 | 1.2 | 2.54 |
| 44.94 | 800 | 112.96 | 0.3 | 1.6 | 1.2 | 3.46 |
| 31.05 | 400 | 39.02 | 0.2 | 2 | 0.8 | 7.24 |
| 33.04 | 600 | 62.29 | 0.2 | 2 | 0.8 | 4 |
| 35.01 | 800 | 88.00 | 0.2 | 2 | 0.8 | 2.32 |
| 37 | 400 | 46.50 | 0.1 | 2 | 0.8 | 3.84 |
| 39.04 | 600 | 73.60 | 0.1 | 2 | 0.8 | 3.74 |
| 40.95 | 800 | 102.93 | 0.1 | 2 | 0.8 | 2.92 |
| 42.96 | 400 | 53.99 | 0.3 | 2 | 0.8 | 3.82 |
| 44.94 | 600 | 84.72 | 0.3 | 2 | 0.8 | 3.86 |
| 46.93 | 800 | 117.96 | 0.3 | 2 | 0.8 | 1.58 |

Table 5.2 Result of Regression Analysis

Regression Analysis: log Ra versus log V, log f, log d, log NR

The regression equation is

log Ra = 2.15 - 0.662 log V + 0.427 log f - 0.504 log d - 0.102 log NR

Predictor        Coef     SE Coef          T        P

Constant       2.1451      0.2971       7.22    0.000

log V         -0.6623      0.1486      -4.46    0.000

log f          0.4267      0.1134       3.76    0.000

log d         -0.5037      0.1156      -4.36    0.000

log NR        -0.1017      0.1127      -0.90    0.370

S = 0.2008      R-Sq = 39.8%     R-Sq(adj) = 36.6%

Analysis of Variance

Source            DF          SS          MS         F        P

Regression         4     2.02407     0.50602     12.55    0.000

Residual Error    76     3.06404     0.04032

Total             80     5.08811

Source       DF      Seq SS

log V         1     0.65624

log f         1     0.57009

log d         1     0.76489

log NR        1     0.03285

Obs      log V     log Ra         Fit      SE Fit    Residual    St Resid

1       1.59     0.6300      0.9097      0.0617     -0.2797       -1.46

2       1.79     0.7900      0.7772      0.0490      0.0128        0.07

3       1.95     0.6900      0.6713      0.0505      0.0187        0.10

4       1.67     0.5700      0.7287      0.0607     -0.1587       -0.83

5       1.87     0.6100      0.5962      0.0567      0.0138        0.07

6       2.01     0.5900      0.5035      0.0628      0.0865        0.45

7       1.73     0.9600      0.8938      0.0576      0.0662        0.34

8       1.93     0.8100      0.7613      0.0549      0.0487        0.25

9       2.07     0.7800      0.6686      0.0621      0.1114        0.58

10       1.59     0.6800      0.7334      0.0541     -0.0534       -0.28

11       1.79     0.5100      0.6009      0.0393     -0.0909       -0.46

12       1.94     0.4900      0.5016      0.0407     -0.0116       -0.06

13       1.66     0.4100      0.5590      0.0537     -0.1490       -0.77

14       1.86     0.3100      0.4266      0.0484     -0.1166       -0.60

15       2.01     0.1100      0.3272      0.0556     -0.2172       -1.13

16       1.73     0.8500      0.7175      0.0495      0.1325        0.68

17       1.93     0.8000      0.5850      0.0465      0.2150        1.10

18       2.07     0.8000      0.4923      0.0549      0.3077        1.59

19       1.59     0.6800      0.6830      0.0573     -0.0030       -0.02

20       1.79     0.5700      0.5506      0.0436      0.0194        0.10

21       1.94     0.5300      0.4512      0.0449      0.0788        0.40

22       1.67     0.3800      0.5020      0.0563     -0.1220       -0.63

23       1.86     0.2200      0.3762      0.0519     -0.1562       -0.81

24       2.01     0.0600      0.2768      0.0588     -0.2168       -1.13

25       1.73     0.9000      0.6671      0.0530      0.2329        1.20

26       1.93     0.8200      0.5347      0.0502      0.2853        1.47

27       2.07     0.8500      0.4419      0.0581      0.4081        2.12R

28       1.60     0.7600      0.8725      0.0534     -0.1125       -0.58

29       1.79     0.7000      0.7467      0.0395     -0.0467       -0.24

30       1.94     0.3100      0.6474      0.0409     -0.3374       -1.72

31       1.67     0.6800      0.6982      0.0533     -0.0182       -0.09

32       1.87     0.6400      0.5657      0.0488      0.0743        0.38

33       2.01     0.4300      0.4730      0.0557     -0.0430       -0.22

34       1.73     0.8400      0.8633      0.0498     -0.0233       -0.12

35       1.93     0.5300      0.7308      0.0467     -0.2008       -1.03

36       2.07     0.4300      0.6381      0.0550     -0.2081       -1.08

37       1.59     0.7500      0.7029      0.0457      0.0471        0.24

38       1.79     0.5000      0.5704      0.0265     -0.0704       -0.35

39       1.94     0.1900      0.4711      0.0287     -0.2811       -1.41

40       1.67     0.5500      0.5219      0.0444      0.0281        0.14

41       1.87     0.4100      0.3894      0.0390      0.0206        0.10

42       2.01     0.2700      0.2967      0.0475     -0.0267       -0.14

43       1.73     0.4900      0.6870      0.0402     -0.1970       -1.00

44       1.93     0.1500      0.5545      0.0364     -0.4045       -2.05R

45       2.07     0.4100      0.4618      0.0467     -0.0518       -0.27

46       1.59     0.4800      0.6342      0.0551     -0.1542       -0.80

47       1.79     0.1400      0.5017      0.0406     -0.3617       -1.84

48       1.94     0.2500      0.4024      0.0422     -0.1524       -0.78

49       1.67     0.4800      0.4532      0.0540      0.0268        0.14

50       1.86     0.4000      0.3274      0.0495      0.0726        0.37

51       2.01     0.0900      0.2280      0.0567     -0.1380       -0.72

52       1.73     0.4000      0.6183      0.0506     -0.2183       -1.12

53       1.93     0.1900      0.4858      0.0477     -0.2958       -1.52

54       2.07     0.1900      0.3931      0.0560     -0.2031       -1.05

55       1.59     0.7000      0.8609      0.0596     -0.1609       -0.84

56       1.79     0.8300      0.7284      0.0464      0.1016        0.52

57       1.94     0.7400      0.6291      0.0477      0.1109        0.57

58       1.67     0.7200      0.6798      0.0586      0.0402        0.21

59       1.87     0.4700      0.5474      0.0545     -0.0774       -0.40

60       2.01     0.6000      0.4547      0.0609      0.1453        0.76

61       1.72     1.7200      0.8516      0.0560      0.8684        4.50R

62       1.93     0.6600      0.7125      0.0527     -0.0525       -0.27

63       2.07     0.5600      0.6198      0.0602     -0.0598       -0.31

64       1.59     0.8100      0.6846      0.0518      0.1254        0.65

65       1.80     0.7000      0.5455      0.0357      0.1545        0.78

66       1.94     0.6800      0.4528      0.0377      0.2272        1.15

67       1.67     0.6500      0.5036      0.0506      0.1464        0.75

68       1.87     0.7200      0.3711      0.0460      0.3489        1.79

69       2.01     0.5200      0.2784      0.0534      0.2416        1.25

70       1.73     0.7700      0.6687      0.0470      0.1013        0.52

71       1.91     0.4000      0.5495      0.0432     -0.1495       -0.76

72       2.05     0.5400      0.4567      0.0510      0.0833        0.43

73       1.59     0.8600      0.6525      0.0494      0.2075        1.07

74       1.79     0.6000      0.5201      0.0325      0.0799        0.40

75       1.94     0.3700      0.4207      0.0344     -0.0507       -0.26

76       1.67     0.5800      0.4715      0.0482      0.1085        0.56

77       1.87     0.5700      0.3390      0.0434      0.2310        1.18

78       2.01     0.4700      0.2463      0.0512      0.2237        1.15

79       1.73     0.5800      0.6366      0.0444     -0.0566       -0.29

80       1.93     0.5900      0.5041      0.0410      0.0859        0.44

81       2.07     0.2000      0.4114      0.0504     -0.2114       -1.09

R denotes an observation with a large standardized residual

Surface roughness equation

The data of analysis of variance of the roughness model shown in table 5.2 the surface roughness model developed as:

logRa=139.669−0.6623 log V+0.4267 log f−0.5037 log d−0.1017 log NR	(5.15)

Equation formulated from the above model is:

Ra=139.669 V−0.6623 f0.4267 d−0.5037 NR−0.1017			(5.16)

The R-square value of 38.9% indicated the variability in the surface roughness was explained by the model with factors V, f and d. based on the mathematical model, it can be concluded that the cutting speed is a dominant factor in the roughness model of finish turning in heavy machining operation.

Chapter 6

RESULTS AND CONCLUSION

This work presented an experimentation approach to studying the impact of machining parameters on surface roughness. Strong interactions were observed among the machining turning parameters. Most significant interactions were found between work materials, feed and cutting speeds. A systematic approach was provided to design and analyze the experiments, which is able to reduce the cost and time of experiments and to utilize the data obtained to the maximum extend.

From the data collection we have observed that the increase in cutting speed tends to improve the finish, thus the average surface roughness value decreases. The increase in depth of cut influences the finish slightly, but greater depth of cut marks the finish poor. Feed rate is the most critical parameter when finish is the criterion. Finish gets poor as the feed increases, thus the average surface roughness value increases with increase in feed.

We have developed the regression models for the non-linear case.

Table 6.1 Comparison of actual and calculated surface roughness

| Diameter (mm) | RPM | Cutting Speed (m/min) | Feed (mm/rev) | Depth of cut (mm) | Nose Radius (mm) | Actual Ra (μm) | Calculated Ra (μm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30.92 | 400 | 38.86 | 0.2 | 1.6 | 0.4 | 4.82 | 5.39 |
| 32.85 | 600 | 61.93 | 0.2 | 1.6 | 0.4 | 3.2 | 3.96 |
| 34.83 | 800 | 87.55 | 0.2 | 1.6 | 0.4 | 3.1 | 3.15 |
| 36.79 | 400 | 46.24 | 0.1 | 1.6 | 0.4 | 2.58 | 3.58 |
| 38.77 | 600 | 73.09 | 0.1 | 1.6 | 0.4 | 2.02 | 2.64 |
| 40.75 | 800 | 102.43 | 0.1 | 1.6 | 0.4 | 1.28 | 2.11 |
| 42.85 | 400 | 53.85 | 0.3 | 1.6 | 0.4 | 7.12 | 5.16 |
| 44.76 | 600 | 84.38 | 0.3 | 1.6 | 0.4 | 6.36 | 3.84 |
| 46.74 | 800 | 117.49 | 0.3 | 1.6 | 0.4 | 6.36 | 3.08 |
| 31.06 | 400 | 39.04 | 0.2 | 0.7 | 0.4 | 4.3 | 8.15 |
| 33.03 | 600 | 62.27 | 0.2 | 0.7 | 0.4 | 6.16 | 5.98 |
| 35.11 | 800 | 88.25 | 0.2 | 0.7 | 0.4 | 4.86 | 4.75 |
| 37.1 | 400 | 46.63 | 0.1 | 0.7 | 0.4 | 3.72 | 5.39 |
| 39.05 | 600 | 73.62 | 0.1 | 0.7 | 0.4 | 4.04 | 3.98 |
| 40.97 | 800 | 102.98 | 0.1 | 0.7 | 0.4 | 3.86 | 3.19 |
| 43 | 400 | 54.04 | 0.3 | 0.7 | 0.4 | 9.02 | 7.81 |
| 45.05 | 600 | 84.93 | 0.3 | 0.7 | 0.4 | 6.44 | 5.79 |
| 47.03 | 800 | 118.21 | 0.3 | 0.7 | 0.4 | 6.02 | 4.65 |
| 30.93 | 400 | 38.87 | 0.2 | 2 | 0.4 | 4.8 | 4.82 |
| 32.88 | 600 | 61.99 | 0.2 | 2 | 0.4 | 3.7 | 3.54 |
| 34.87 | 800 | 87.65 | 0.2 | 2 | 0.4 | 3.38 | 2.81 |
| 36.81 | 400 | 46.26 | 0.1 | 2 | 0.4 | 2.38 | 3.19 |
| 38.82 | 600 | 73.18 | 0.1 | 2 | 0.4 | 1.66 | 2.36 |
| 40.79 | 800 | 102.53 | 0.1 | 2 | 0.4 | 1.16 | 1.89 |
| 42.83 | 400 | 53.83 | 0.3 | 2 | 0.4 | 7.86 | 4.62 |
| 44.83 | 600 | 84.51 | 0.3 | 2 | 0.4 | 6.66 | 3.42 |
| 46.78 | 800 | 117.59 | 0.3 | 2 | 0.4 | 7.1 | 2.75 |
| 31.8 | 400 | 39.97 | 0.2 | 0.7 | 0.8 | 5.78 | 7.48 |
| 32.99 | 600 | 62.19 | 0.2 | 0.7 | 0.8 | 5.06 | 5.58 |
| 34.95 | 800 | 87.85 | 0.2 | 0.7 | 0.8 | 2.04 | 4.44 |
| 36.9 | 400 | 46.38 | 0.1 | 0.7 | 0.8 | 4.82 | 5.04 |
| 38.89 | 600 | 73.32 | 0.1 | 0.7 | 0.8 | 4.34 | 3.72 |
| 40.9 | 800 | 102.81 | 0.1 | 0.7 | 0.8 | 2.68 | 2.98 |
| 42.89 | 400 | 53.90 | 0.3 | 0.7 | 0.8 | 6.92 | 7.29 |
| 44.9 | 600 | 84.65 | 0.3 | 0.7 | 0.8 | 3.4 | 5.41 |
| 46.88 | 800 | 117.84 | 0.3 | 0.7 | 0.8 | 2.68 | 4.35 |
| 31 | 400 | 38.96 | 0.2 | 1.6 | 0.8 | 5.66 | 5.02 |
| 32.98 | 600 | 62.17 | 0.2 | 1.6 | 0.8 | 3.14 | 3.68 |
| 34.97 | 800 | 87.90 | 0.2 | 1.6 | 0.8 | 1.54 | 2.93 |
| 36.98 | 400 | 46.48 | 0.1 | 1.6 | 0.8 | 3.52 | 3.32 |
| 38.89 | 600 | 73.32 | 0.1 | 1.6 | 0.8 | 2.56 | 2.46 |
| 40.89 | 800 | 102.78 | 0.1 | 1.6 | 0.8 | 1.88 | 1.96 |
| 42.99 | 400 | 54.03 | 0.3 | 1.6 | 0.8 | 3.06 | 4.80 |
| Diameter (mm) | RPM | Cutting Speed (m/min) | Feed (mm/rev) | Depth of cut (mm) | Nose Radius (mm) | Actual Ra (μm) | Calculated Ra (μm) |
| 44.89 | 600 | 84.63 | 0.3 | 1.6 | 0.8 | 1.4 | 3.57 |
| 46.87 | 800 | 117.81 | 0.3 | 1.6 | 0.8 | 2.58 | 2.87 |
| 31 | 400 | 38.96 | 0.2 | 2 | 1.2 | 3.02 | 4.30 |
| 32.92 | 600 | 62.06 | 0.2 | 2 | 1.2 | 1.38 | 3.16 |
| 34.89 | 800 | 87.70 | 0.2 | 2 | 1.2 | 1.76 | 2.51 |
| 36.87 | 400 | 46.34 | 0.1 | 2 | 1.2 | 3.02 | 2.85 |
| 38.83 | 600 | 73.20 | 0.1 | 2 | 1.2 | 2.5 | 2.11 |
| 40.81 | 800 | 102.58 | 0.1 | 2 | 1.2 | 1.24 | 1.69 |
| 42.82 | 400 | 53.82 | 0.3 | 2 | 1.2 | 2.5 | 4.13 |
| 44.85 | 600 | 84.55 | 0.3 | 2 | 1.2 | 1.56 | 3.06 |
| 46.84 | 800 | 117.74 | 0.3 | 2 | 1.2 | 1.54 | 2.46 |
| 31.02 | 400 | 38.99 | 0.2 | 0.7 | 1.2 | 4.96 | 7.30 |
| 32.97 | 600 | 62.16 | 0.2 | 0.7 | 1.2 | 6.82 | 5.36 |
| 34.99 | 800 | 87.95 | 0.2 | 0.7 | 1.2 | 5.5 | 4.26 |
| 36.95 | 400 | 46.44 | 0.1 | 0.7 | 1.2 | 5.24 | 4.83 |
| 38.9 | 600 | 73.33 | 0.1 | 0.7 | 1.2 | 2.94 | 3.57 |
| 40.91 | 800 | 102.83 | 0.1 | 0.7 | 1.2 | 3.96 | 2.86 |
| 42.09 | 400 | 52.90 | 0.3 | 0.7 | 1.2 | 52.4 | 7.09 |
| 44.92 | 600 | 84.68 | 0.3 | 0.7 | 1.2 | 4.62 | 5.19 |
| 46.91 | 800 | 117.91 | 0.3 | 0.7 | 1.2 | 3.6 | 4.17 |
| 31.07 | 400 | 39.05 | 0.2 | 1.6 | 1.2 | 6.46 | 4.81 |
| 33.35 | 600 | 62.87 | 0.2 | 1.6 | 1.2 | 5.04 | 3.51 |
| 35.01 | 800 | 88.00 | 0.2 | 1.6 | 1.2 | 4.82 | 2.81 |
| 36.96 | 400 | 46.45 | 0.1 | 1.6 | 1.2 | 4.5 | 3.19 |
| 38.94 | 600 | 73.41 | 0.1 | 1.6 | 1.2 | 5.22 | 2.35 |
| 40.93 | 800 | 102.88 | 0.1 | 1.6 | 1.2 | 3.3 | 1.88 |
| 42.93 | 400 | 53.95 | 0.3 | 1.6 | 1.2 | 5.9 | 4.61 |
| 42.92 | 600 | 80.91 | 0.3 | 1.6 | 1.2 | 2.54 | 3.53 |
| 44.94 | 800 | 112.96 | 0.3 | 1.6 | 1.2 | 3.46 | 2.83 |
| 31.05 | 400 | 39.02 | 0.2 | 2 | 0.8 | 7.24 | 4.48 |
| 33.04 | 600 | 62.29 | 0.2 | 2 | 0.8 | 4 | 3.29 |
| 35.01 | 800 | 88.00 | 0.2 | 2 | 0.8 | 2.32 | 2.61 |
| 37 | 400 | 46.50 | 0.1 | 2 | 0.8 | 3.84 | 2.97 |
| 39.04 | 600 | 73.60 | 0.1 | 2 | 0.8 | 3.74 | 2.19 |
| 40.95 | 800 | 102.93 | 0.1 | 2 | 0.8 | 2.92 | 1.75 |
| 42.96 | 400 | 53.99 | 0.3 | 2 | 0.8 | 3.82 | 4.29 |
| 44.94 | 600 | 84.72 | 0.3 | 2 | 0.8 | 3.86 | 3.19 |
| 46.93 | 800 | 117.96 | 0.3 | 2 | 0.8 | 1.58 | 2.56 |

The present study can be concluded in the following steps:

- For regression equation relationship with the R-square value of 38.9% indicate that the variability in the surface roughness was explained by the model with factors V, f, d and NR.

- A methodology for the prediction of surface roughness in turning using Regression Analysis has been developed. A good number of experiments have been conducted on EN8 work-piece metal using CARBIDE cutting tool material by design of experiment. The optimum network architecture has been found out based on the mean square error and the convergence rate. The predicted surface roughness from the present Regression Analysis model is very close to the values measured experimentally, thus showing the efficacy of Regression Analysis for predicting surface roughness in turning.

Scope for future work

The machining variables are divided into four main categories. These are tool variables, work piece variables and set-up variables.  Tool variables includes tool material, nose radius, tool wear, tool geometry, tool vibration, machine tool rigidity, and tool overhang etc. Work piece variables include work piece material, hardness, length and diameter etc. Set-up variables include cutting speed, feed rate, depth of cut etc. In the present work only set-up variables are considered. Tool variables and work piece variables can also be optimized by using Taguchi design of experiment There is also scope for considering more factors levels, interactions to optimize a selected set of parameters. A comparison between different optimization techniques can also be studied to check which optimization technique is better.

It is also one of the important things to analyze why surface roughness first increases and then decreases with design parameters.

REFERENCES

Choudhury, S. K., Jain V. K.  and Rama Rao, Ch. V. V., 1999, “On-line monitoring of tool wear in turning using a neural network” International Journal of Machine Tools and Manufacture, vol. 39, pp. 489-504

Feng. Cang-Xue (Jack), 2001 “An Experimental Study of the Impact of Turning Parameters on Surface Roughness”. Proceedings of the 2001 Industrial Engineering Research Conference Copyright, Institute of Industrial Engineers, paper no. 2036.

Feng, C. X. and Wang, X, 2002, “Development of empirical models for surface roughness prediction in finish turning”. International Journal of Advanced Manufacturing Technology, vol. 20, pp. 348-356.

Jiao Y, Lei S., Pei Z.J. and Lee E.S., 2004“Fuzzy adaptive networks in machining process modeling: surface roughness prediction for turning operations”. International Journal of Machine Tools & Manufacture, vol. 44, pp. 1643–1651.

Kirby, Zhang and Chen, 2004, “Determining the surface roughness of a work piece using a Federal Pocket Surf stylus profilometer”. Journal of Industrial Technology, vol-20 number-4 date Sept, 2004.

Lambert, B. K., 1983 “Determination of metal removal rate with surface finish restriction”. Carbide and Tool Journal, May- June: 16-19.

Lambert, B. K., and Taraman, K., 1974 A surface roughness model for a turning operation. International Journal of Production Research, vol. 12, pp. 691-703.

Lee S. S. and Chen J. C., 2003 “On-line surface roughness recognition system using artificial neural networks system in turning operations”. International Journal of Advance Manufacturing Technology, vol. 22, pp. 498–509.

Malakooti B. and Raman V., 2000 “An interactive multi-objective artificial neural network approach for machine setup optimization”. Journal of Intelligent Manufacturing, vol. 11, pp. 41-50.

Monostori L., 1993, “A step towards intelligent manufacturing: modelling and monitoring of manufacturing processes through artificial neural network”, Ann CIRP, vol. 42, pp. 485–493.

Ozel,  T. and Karpat, Y., 2004, “Predictive modeling of surface roughness and tool wear in hardturning using regression and neural networks” International Journal of Machine Tools & Manufacture, vol.45, pp. 467–479.

Palanikumar K., Karunamoorthy L. and Karthikeyan R., 2005 “Assessment of factors influencing surface roughness on the machining of glass fiber-reinforced polymer composites” Journal of Materials and Design.

Palanikumar K. and Karthikeyan R., 2007. “Assessment of factors influencing surface roughness on the machining of Al/SiC particulate composites” Journal of Materials and Design, vol. 28, pp. 1584-1591.

Pal, S.K. and Chakraborty, D., 2005 “Surface roughness prediction in turning using artificial neural network”. Springer-Verlag London Limited.

Rasch and Rolstadas, 1971, “Series of finish turning tests under variation of parameters: material quality, tool quality, tool nose radius, feed, speed and cutting time”. Journal of Materials Processing Technology vol-132, pp. 203-214.

Sahin, Yusuf and Motorcu A.Riza., 2004“Surface Roughness Prediction Model in Machining of Carbon Steel by PVD Coated Cutting Tools”. American Journal of Applied Sciences, vol 1, pp. 12-17

Sundaram. R. M., 1976, “A statistical analysis of surface finish in fine turning of steel, unpublished Doctoral Dissertation in Industrial Engineering”, Texas Tech

University Lubbock, TN.

Sundaram, R. M. and Lambert, B. K., 1979, “Surface roughness variability of ANSI 4140 steel in fine turning using carbide tools”. International Journal of Production Research, vol.17, pp. 249-258.

Sundaram, R. M. and Lambert, B. K., 1981, “Mathematical models to predict surface finish in fine turning of steel: Part I and Part II”. International Journal of Production Research, vol. 19, pp. 557-564

Taraman, K. and Lambert, B. K., 1974, “A surface roughness model for a turning operation”, International Journal of Production Research, vol. 12, pp. 691-703.

Wu, S.M. 1964. ‘Tool life testing by Response Surface Methodology-Part1”, Journal of Engineering for Industry. Transactions of ASME, pp. 111.

Yang W.H., Tarng Y.S. 1998 “Design optimization of cutting parameters for turning operations based on the Taguchi method”. Journal of Materials Processing Technology, vol 84, pp. 122–129.

Yeo, S.H., Rahman, M. and Wong, Y.S., 1989, “Towards enhancement of mach inability data by multiple regression”. Journal of Mechanical Working Technology, vol. 19, pp. 85-99.

Yeo, S.H., 1995, “A multipass optimization strategy for CNC lathe operations”. International Journal of Production Economics, vol 40, pp. 209-218.

Zuperl Uros, Cus Franci 2003“Optimization of cutting conditions during cutting by using neural networks”. Robotics and Computer Integrated Manufacturing, vol 19, pp. 189–199.

APPENDIX

Programming of CNC Trainer Lathe

List of G Codes

| CODE | FUNCTION |
| --- | --- |
| G00 | RAPID POSITIONING |
| G01 | LINEAR INTERPOLATION |
| G02 | CLOCKWISE CIRCULAR INTERPOLATION |
| G03 | CONTER CLOCKWISE CIRCULAR INTERPOLATION |
| G04 | DWELL IN SECONDS |
| G20 | INCH PROGRAMMING |
| G21 | METRIC PROGRAMMING |

| G28 | AUTO. RETURN TO REF. POINT |
| --- | --- |
| G32 | THREAD CUTTING CYCLE |
| G70 | FINISHING CYCLE |
| G71 | STOCK REMOVAL IN TURNING |
| G72 | STOCK REMOVAL IN FACING |
| G73 | PATTERN REPEATING CYCLE |
| G74 | PECK DRILLING CANNED CYCLE |
| G90 | DAIMETER CUTTING CYCLE |
| G94 | FACING CANNED CYCLE |
| G96 | CONSTANT SURAFCE SPEED ON |

List of M Codes

| CODE | FUNCTION |
| --- | --- |
| M00 | PROGRAM STOP |
| M01 | OPTIONAL PROGRAM STOP |
| M02 | PROGRAM END |
| M03 | SPINDLE START CLOCKWISE |
| M04 | SPINDLE START ANTICLOCKWISE |
| M05 | SPINDLE STOP |
| M07 | COOLANT NO. 1 ON |
| M08 | COOLANT NO.2 ON |
| M09 | COOLANT OFF |
| M13 | SPINDLE CLOCKWISE & COOLANT ON |

| M14 | SPINDLE ANTI-CLOCKWISE & COOLANT ON |
| --- | --- |
| M30 | PROGRAM END & REWIND |
| M98 | START OF SUBROUTINE |
| M99 | END OF SUBROUTINE |

BIBLIOGRAPHY

1. Surface Roughness Terminology:

The quality of machined surface is characterized by the accuracy of its manufacture with respect to the dimensions specified by the designer. Every machining operation leaves characteristic evidence on the machined surface. This evidence in the form of finely spaced micro irregularities left by the cutting tool. Each type of cutting tool leaves its own individual pattern which therefore can be identified. This pattern is known as surface finish or surface roughness.

2. Roughness:

Roughness consists of surface irregularities which result from the various machining process. These irregularities combine to form surface texture.

### 3. Roughness Height:

It is the height of the irregularities with respect to a reference line. It is measured in millimeters or microns or micro inches. It is also known as the height of unevenness.

### 4. Roughness Width:

The roughness width is the distance parallel to the nominal surface between successive peaks or ridges which constitute the predominate pattern of the roughness. It is measured in millimeters.

5. Roughness Width Cut Off:

Roughness width cut off is the greatest spacing of respective surface irregularities to be included in the measurement of the average roughness height. It should always be greater than the roughness width in order to obtain the total roughness height rating.

6. Lay:

Lay represents the direction of predominant surface pattern produced and it reflects the machining operation used to produce it.

7. Waviness:

This refers to the irregularities which are outside the roughness width cut off values. Waviness is the widely spaced component of the surface texture. This may be the result of work piece or tool deflection during machining, vibrations or tool run out.

8. Waviness Width:

Waviness height is the peak to valley distance of the surface profile, measured in millimeters.

9. Arithmetic Average (AA):

A close approximation of the arithmetic average roughness-height can be calculated from the profile chart of the surface. Averaging from a mean centerline may also be automatically performed by electronic instruments using appropriate circuitry through a meter or chart recorder. If X is the measured value from the profilometer, then the AA value can be calculated as shown below.

10. Root Mean Square (rms):

The rms value can be calculated as shown below. Its numerical value is about 11% higher than that of AA.

11. Cut-off value

The cut-off value controls the measurement length. For example, if an 0.8mm cut-off is selected and 7 sample lengths are measured, then the measurement length will be 7 x 0.8=5.6mm. In general for good statistical analysis, it is recommended that 5 sample lengths be used for assessment, although this is not always possible. If a 2CR filter is used, then 2 cut-offs will be discarded. This means the measurement length for a 2CR type filter will have to be 7 x 0.8 to allow for the 2 discarded cut-offs leaving a final 5 sample lengths for assessment. The Gaussian type filter is different and only discards one sample length.

12. Spacing Parameters

RSm is the mean spacing between profile peaks as they pass through the mean line (spacing is the distance between points that cross the mean line within a sample length in

an upward direction.

HSC - The high spot count is the number of complete profile peaks (within an assessment length) projecting above a horizontal reference line, in other words, parallel with the mean line. The reference line can be set at a selected distance above or below the mean line.

RPc - The peak count is the number of local peaks which project through a selectable band centered about the mean line. The count is determined only over the assessment length though the results are given in peaks per cm (or per inch). The peak count is obtained by using a multiplication factor. The parameter should, therefore, be measured over the greatest assessment length possible.

13. Stylus Tip Radius

The stylus tip radius is a key feature that is often overlooked. Assuming that a conisphere stylus is being used, the profile recorded by the instrument will in effect be the locus of the centre of a ball, whose radius is equal to that of the stylus tip, as it is rolled over the surface. This action broadens the peaks of the profile and narrows the valleys. For simplicity, if we consider the surface to be a sine wave, then this distortion is dependent both on the wavelength and the amplitude.