A

DISSERTATION

ON

BOND STRENGTH OF RECYCLED AGGREGATE

SUBMITTED IN FULFILLMENT OF THE REQUIREMENT

FOR THE AWARD OF THE DEGREE OF

MASTER OF ENGINEERING

(Structure Engineering)

SUBMITTED BY:

PARDEEP SINDHU

COLLEGE ROLL NO: 014/STR/08

UNIVERSITY ROLL NO. 8493

Under the esteemed Guidance of:

DR. A.K.GUPTA

(ASSISTANT PROFESSOR)

DEPARTMENT OF CIVIL AND ENVIRONMENTAL ENGINEERING

DEPARTMENT OF CIVIL AND ENVIRONMENTAL ENGINEERING

DELHI COLLEGE OF ENGINEERING

UNIVERSITY OF DELHI

2008-2010

CERTIFICATE

This is to declare that the major project on “BOND STRENGTH OF RECYCLED AGGREGATE ” is a bonafide   record of work done by me for partial fulfillment of award of degree in M.E. Civil Engineering (Structural Engineering) at Delhi collage of Engineering.

This project has been carried out under the supervision of Dr. A.K.Gupta, Assistant     Professor, Delhi Collage Engineering.

The work embodied in this major project has not been submitted to any other Institute/University for the award of any other Degree or Diploma.

PARDEEP SINDHU

COLLEGE ROLL NO: 014/STR/08

UNIVERSITY ROLL NO. 8493

Dr. A.K.GUPTA

Assistant Professor

Department of Civil And Environmental Engineering.

Delhi College of Engineering,

University of Delhi, India

ACKNOWLEDGEMENT

It is distinct pleasure to express my deep sense of gratitude and indebtedness to my  supervisor Dr. A.K.GUPTA Assistant Professor, Department of Civil and Environmental Engineering, Delhi College of Engineering, for his invaluable guidance, encouragement and patient reviews. His continuous inspiration only has made me complete this dissertation. Without his help and guidance, this dissertation would have been impossible. He remained a pillar of help throughout the project.

I express my sincere gratitude to the faculty and non teaching staff of civil and Environmental engineering department and the library of Delhi College of Engineering for providing the relevant information and help when needed during the course of my this project work.

I am very thankful to Dr.V.K.Shagal, Professor NIT Kuruksheta for allow me to test my specimen in there lab.

I am also thankful to my classmates and my friends for their unconditional support and motivation during this work

I am grateful to my Father for mentoring me, my Mother  and my family for being my moral support all the time; they have been always around to guide and cheer me up, in the odd times of this work.

PARDEEP SINDHU

ABSTRACT

The objective of this study is to use of recycled aggregate as replacement of natural aggregate for saving the natural resources and energy. Recycled aggregates consist of crushed, graded inorganic particles processed from the materials that have been used in the constructions and demolition debris. The aim for this present work is to determine the strength characteristic of recycled aggregates for application in structural concrete. The scope of the thesis is to determine and compare the bond strength of concrete by prepared by natural aggregate and recycled aggregate. The investigation was carried out using workability test, compressive strength test, indirect tensile test, and bond strength test. A total of six mixes three from natural coarse aggregate with mix proportion of 1:1.87:3.24, 1:1.59:2.75 & 1:1.41:2.41with w/c 0.45, 0.39 & 0.34 respectively and remaining three were prepared in same ratio with recycled coarse aggregate. A water reducing admixture was used at 1% of weight of cement. It was observed that the workability of concrete reduces with use of recycled aggregate. For strength characteristics, the result showed a slight decrease in compressive strength, tensile strength and bond strength as the percentage of recycled aggregate is increased.

List of Notations

A	-	Aggregate

BIS	-	Bureau of Indians Standard

C	-	Cement

CA	-	Coarse Aggregate Ratio

C/A	-	Cement Aggregate Ratio

C.F.	-	Compaction Factor

FA	-	Fine Aggregate

FRP	-	Fibre Reinforced Polymer

NCA	-	Natural Coarse Aggregate

OPC	-	Ordinary Portland Cement

RAC	-	Recycled Aggregate Concrete

RCC	-	Reinforced Cement Concrete

SCC	-	Self Compacting Concrete

SD	-	Standard Deviation

VC	-	Vibrated Concrete

W	-	Water

W/C	-	Water Cement Ratio

List of Tables

TABLE			DESCRIPTION			               	      PAGE

3.1			Physical properties of cement 43-grade			19

3.2 (a)		Sieve Analysis of Natural Fine Aggregate			20

3.2 (b)		Physical Properties of Natural Fine Aggregate		20

3.3 (a)		Sieve Analysis of Coarse Aggregate (10 mm)		21

3.3 (b)		Physical Properties of Coarse Aggregate (10 mm) 		21

3.4 (a)		Sieve Analysis of Coarse Aggregate (20 mm)		22

3.4 (b)		Physical Properties of Coarse Aggregate (20 mm) 		22

3.5 (a)		Sieve Analysis of Recycled Aggregate			23

3.5 (b)		Physical Properties of Recycled Aggregate			23

3.6			Mix proportion							24

3.7			Size of Moulds							25

3.8			Properties of Fresh concrete				          26

4.1			Compressive Strength at different ages (1:1.87:3.24)	31

4.2			Compressive Strength at different ages (1:1.59:2.75)         32

4.3                          Compressive Strength at different ages (1:1.4:2.41)		 33

4.4			Tensile Strength at different ages (1:1.87:3.24)		 36

4.5			Tensile Strength at different ages (1:1.59:2.75)		   37

4.6			Tensile Strength at different ages (1:1.4:2.41)		   38

4.7			Bond Strength at different ages (1:1.87:3.24)			   42

4.8			Bond Strength at different ages (1:1.59:2.75)			   43

4.9		          Bond Strength at different ages (1:1.4:2.41)                          44

5.1                          Comparison of property of  different mix                              49

List of figures

FIGURE				DESCRIPTION				     PAGES

1.1   Picture show the polluted crusher zone in NCR                                     4

1.2    Dry bed of Badhkal lake in Faridabad in NCR                                      5

1.3    Mining cause formation of large no of water bodies                              6

1.4     Thousands of acer land destroyed due mining                                      7

3.1    Compression testing machine at D.C.E                                                 27

3.2    Tensile testing of cylinder in CTM in D.C.E.                                         28

3.3     Tensile failure of specimen                                                                   29

3.4      Universal testing machine in N.I.T. Kurukshtera                                30

4.1	Variation of Compressive Strength with ages (1:1.87:3.24)                 31

4.2	Variation of Compressive Strength with ages (1:1.59:2.75)	             32

4.3	Variation of Compressive Strength with ages ( 1:1.4:2.41)                  33

4.4	Variation of Compressive Strength of different mix at 3 days             34

4.5	Variation of Compressive Strength of different mix at 7 days             34

4.6    	Variation of Compressive Strength of different mix at 14 days           35

4.7    	Variation of Compressive Strength of different mix at 28 days           35

4.8	Variation of Tensile Strength with age (1:1.87:3.24)          	              37

4.9     Variation of tensile Strength with ages (1:1.59:2.75)	                       38

4.10	Variation of tensile Strength with ages ( 1:1.4:2.41)                               39

4.11	Variation of tensile Strength of different mix at 3 days                           39

4.12	Variation of tensile Strength of different mix at 14 days                         40

4.13  	Variation of tensile Strength of different mix at 28 days                              41

4.14	Variation of Bond Strength with age (1:1.87:3.24)          	                      42

4.15    Variation of Bond Strength with ages (1:1.59:2.75)	                          43

4.16	 Variation of Bond Strength with ages (1:1.4:2.41)                                44

4.17  	Variation of Bond Strength of different mix at 14 days                                45

4.18  	Variation of Bond Strength of different mix at 28 days                           45

CONTENTS

Certificate											         i

Acknowledgement										        ii

Abstract											      iii

List of Notation										       iv

List of Tables										        v

List of Figures										      vii

CHAPTER 1	INTRODUCTION					                 1

1.1	General						                 1

1.2	Historical Background and Developments 	                 2

1.3     Environment prospect                                                    3

1.4	Prospects in India					                  8

1.5	Economic Feasibility				                 8

1.6	Scope of Investigation				                 9

1.7	Organization of Dissertation			                 9

CHAPTER 2	LITERATURE REVIEW				                11

2.1	General						                11

2.2	Review of Literature				                12

2.3	Discussion on Literature Review		                17

2.4	Summary						                17

CHAPTER 3	EXPERIMENTAL PROGRAMME		                          13

3.1	 General						                18

3.2	 Material properties                                                    18

3.2.1	 Cement			                                             18

3.2.2	  Natural fine aggregate			                          19 			 3.2.3	  Natural coarse aggregate                                           21

3.2.4	  Coarse aggregate from demolished 	                          22

concrete

3.2.5	  Water			                                               24

3.3	  Mix proportion			                                    24

3.4     Casting of Specimens		                                   24

3.5      Preparation of concrete from demolished	                25

concrete aggregate

3.5.1   Source of Demolished Concrete		                25

Aggregate

3.5.2   Preparation of Aggregate from		                          25

Demolished Concrete

3.5.3   Processing of demolished concrete                           25

aggregate

3.5.4  Mixing and compaction			                          25

3.6    Properties of Fresh Concrete ( Workability )                 26

3.7    Testing Procedure			                     	      27

3.7.1  Compressive strength				                27

3.7.2   Split Tensile strength				                28

3.7.3   Bond Strength by pull-out test				      29

3.8	Summary							      30

CHAPTER 4    RESULTS AND DISCUSSION OF RESULTS		      31

4.1	General							      31

4.2	Variation of Compressive Strength with

age

4.3	Variation of Tensile Strength with age			      36

4.4	Variation of Bond Strength with age			      41

CHAPTER 5	CONCLUSIONS & SCOPE					      47

5.1	Conclusions							      47

5.2	Scope for Further Study					      49

REPERENCES										      51

APPENDIX I