CERTIFICATE

This is to certify that the thesis entitled, “STUDIES ON THE AGRO BASED FATTY ACIDS EPOXY RESINS AND THEIR COMPOSITES” which is being submitted by Ms. Anshu Dev for the award of the degree of Doctor of Philosophy to the Faculty of Technology, University of Delhi, Delhi, India is entirely based on the experimental work carried out by her under my supervision. The work reported in this thesis embodies the work of the candidate herself and is original one, has not been submitted to any other University or Institution for the award of any degree or diploma

| Dr. A. P. Gupta Supervisor Department of Applied Chemistry & Polymer Technology Delhi College of Engineering Faculty of Technology New Campus, Bawana Road (University of Delhi) Delhi-110042, India | Prof. A Trivedi Dean: Faculty of Technology Head: Dept. of Applied Sciences & Humanities Faculty of Technology University of Delhi (Delhi College of Engineering) (New Campus, Bawana Road) Delhi India |
| --- | --- |

DEPARTMENT OF APPLIED CHEMISTRY AND POLYMER TECHNOLOGY

DELHI COLLEGE OF ENGINEERING, UNIVERSITY OF DELHI

DELHI-110042

INDIA

CERTIFICATE

This is to certify that the thesis, “STUDIES ON THE AGRO BASED FATTY ACIDS EPOXY RESINS AND THEIR COMPOSITES” which is being submitted for the award of the degree of Doctor of Philosophy to the Faculty of Technology, University of Delhi is based on experimental work carried out by me under the supervision of Dr. A.P. Gupta, Department of Applied Chemistry & Polymer Technology, Delhi College of Engineering, (University of Delhi), Delhi, India. The results embodied in the thesis have not been submitted to any University or Institution for the award of any degree or diploma.

(Dr. A. P. Gupta) 								(Anshu Dev)

Supervisor									 Candidate

Dept. of Applied Chemistry and Polymer Technology

Delhi College of Engineering, (University of Delhi)

New Campus, Bawana Road

Delhi-110042

India

ACKNOWLEDGMENTS

I wish to express my deep sense of gratitude to Dr. A. P. Gupta (supervisor) Department of Applied Chemistry & Polymer Technology, Delhi College of Engineering (University of Delhi), Delhi, India for his guidance, keen interest, constructive criticism and valuable suggestion throughout the course of the investigations.

I feel highly indebted to extend my deep sense of gratitude to Prof. Sharif Ahmad, Department of Materials Chemistry, Jamia Millia Islamia, Delhi, India under whose meticulous guidance and constant encouragement this work has achieved its present form.

My sincere thanks are due to Prof. P.  B. Sharma, Director, Delhi College of Engineering, Delhi for constant encouragement and keen interest in the present work.

I owe my sincere thanks to Dr. G. L. Verma, Professor, Head of the Department, Dr. R. C. Sharma and Sh. S. G. Warkar (Lecturer) providing all the facilities. I am also thankful to the librarian Sh. R. K. Shukla and all the library members, of, Delhi College of Engineering (University of Delhi), Delhi.

I take the pleasure for thanking to Sh. B.K. Sharma, Sh. R.S. Chauhan, Sh. Ishwar Singh, Sh. Jeewanram the technical supporting staff of Applied Chemistry Department, Delhi College of Engineering for their full cooperation during the course.

I will always remain thankful to all my colleague and friends, who helped me during the course of my research work. I would like to pay my thanks to Anshu, , Indrani, Gopal and Prasun for their indispensable help and creative suggestions during my research work.

It will be very difficult for me to carry the whole research work without the strong support of my whole family, who all the way have supported me to proceed my research work beside all constraints and its only with their blessings and moral support that enabled me to finish this difficult task with an divine edge. It’s the strong support from all of my family members, especially my Father, Mother, Brother, Husband; who used to study along with me during research study hours so as make me remember that I must study more and absolutely the blessings of my grandmother that always made me to wade through all situations to reach the final goal. It’s their wide adaptability, strong ethical support and faith in me that made me to gain an easy outlook over the whole problem. It’s the gracious blessing of God that made to realize the truth and follow me to precede the right path for acquiring few pebbles of knowledge from its seashore.

Place- Delhi								 	(Anshu Dev)

Date- 										  Candidate

ABSTRACT

The increasing environmental regulations generated by disposal of conventional plastics and related polymers from petrochemicals have intensified researches into polymers that have their origin from annually renewable resources such as plant oils, cellulose and lactic acid. As part of the solution to these problems concerted efforts are being made by scientists and researchers in both research and educational institutions to design novel products possessing acceptable qualities.

Polymer composites manufactured by using agro based plant/crop oil as matrices and bio-fibers such as flax, hemp, sisal, kenaf and wood, as reinforcements are having the capability of recycling, commercial viability and environmental acceptability with triggered biodegradability defined as “Sustainable” agro based products.

The most interesting raw material candidates for bio-based thermosets can be found among the plant oils. The plant oils are triglycerides, composed of glycerol combined with fatty acids into an ester. There are many sources for plant oils, and these can be grown almost all over the world. Soybean, linseed, rape seed, corn, canola, palm or sun flower are some oils. For their use in thermosets the triglyceride compound must be isolated and purified, and also functionalized to obtain reactivity. The plant oil is then cross-linked in a similar manner as crude oil based thermosets. Various chemical modifications for the plant oil are possible; and they utilize the unsaturated double bonds in the fatty acid part of the triglyceride.

In this contribution we will describe the use of agro based chemically modified plant oil i.e., epoxidized soybean oil (ESO) via the epoxidation of the unsaturation present in the hydrocarbon chain. The objectives of this research work are to develop new epoxidized soybean oil (ESO) based polymers. The research work is divided in three parts:

- Optimization of anhydride/epoxy ratio.

- Modification of ESO by addition of a co-monomer.

- Preparation of ESO based composites.

This will surely increases the demand of epoxidized soybean oil as raw material for industrial applications. Various characterization techniques used to the study of mechanical, thermo-mechanical, thermal and morphological properties of the different systems.

The variation in anhydride to epoxy stoichiometric ratios permits the control of thermo-physical properties along with the thermal properties over a wide range. The storage modulus, glass transition temperature, and cross-link density increased with an increase in the hardener content and reaches maximum at stoichiometric equivalence and decreases further. In contrast the izod impact strength and thermal stability shows monotonic behavior. This is further supported by SEM micrographs. All these results concluded that the anhydride/epoxy, ratio R = 1 works best. Our data supports the contention that any deviation from stoichiometry lowers the properties because a negative departure from stoichiometry results in a less improved network.

The variation of DGEBA content was used to modify the epoxidized soybean oil (ESO) and the modified system shows the properties corresponding to the amount of modifier (DGEBA).From DMA, FTIR, mechanical properties, SEM and TGA results, it was concluded that properties were enhanced only up to 20phr DGEBA. Thus 10 and 20 phr DGEBA works best and approached to an ideal composition which gives the optimum property. Thus, at lower concentration of modifier, properties characteristic to ESO, which is soft and flexible with higher impact property, were obtained.  At higher concentration of modifier, system obey property characteristic to DGEBA, which is inherently brittle.

The silane treatment effectively increases the thermo-mechanical properties of the composites. In silane treated fiber, the interpenetration of the coupling agent into the cell wall of fibers through pores and its deposition in the inter-fibrillar region, generating a barrier that hinders the moisture access to fibers and reduces its hydrophilic nature. And finally improves the properties.

From DMA, mechanical properties, SEM and TGA, it was observed that with increasing fiber content  in ESO-untreated fiber composites gives declined Tg, increasing mechanical properties, poor adhesion and lower thermal stability. In case of ESO-silane treated fiber composites, from DMA, mechanical properties, SEM and TGA, it was observed that with increasing fiber content  Tg was increased, mechanical properties were improved, better adhesion and higher thermal stability. All these properties were higher than untreated fiber composites. For both the composite systems, composites at 1.5 wt% fiber loading give the optimum properties and works best.

Again from DMA, mechanical properties, SEM and TGA, it was observed that with increasing fiber content in ESO/DGEBA (10)-untreated fiber composites gives declined Tg but improved mechanical properties, poor adhesion and lower thermal stability.  From DMA, mechanical properties, SEM and TGA, it was observed that with increasing fiber content  ESO/DGEBA (10)-silane treated fiber composites gives  increasing Tg, increasing mechanical, better adhesion and higher thermal stability. All these properties were higher than untreated fiber composites. For ESO/DGEBA (10)-untreated fiber system, composites at 1.5 wt% fibers loading gives the optimum properties whereas for ESO-silane treated system, 2.5 wt% composite works best.

Thus the developed ESO based polymer systems and composites would be interesting alternative, derived as biomaterials from renewable resources. And the widening of the range of properties is very important for future studies. Therefore it is hoped that the results described will be useful for a state- of-art- designing of suitable ESO based polymers and composites.

List of Figures

Figure 1.1 :  Changing sources of feedstock for the chemical industry.	2

Figure 1.2  :  Triglyceride molecule, the major component of plant oils.	3

Figure 1.3 :  Reactive positions in triglycerides: (a) ester groups, (b) c=c double 	4

Figure 1.4 :  Reaction of triglyceride with acrylic acid.	8

Figure 1.5 :  Epoxidation of triglyceride.	9

Figure 1.6 :  Reaction of triglyceride with an acid.	10

Figure 1.7 :  Reaction of triglyceride with cinnamic acid.	10

Figure 1.8 :  Reaction of triglyceride with maleic anhydride	12

Figure 1.9 :  Conversion of triglycerides to mono and di-glycerides.	12

Figure 1.10: Reaction of triglyceride with acrylonitrile.	13

Figure 1.11 : Structure of an elementary plant fiber (cell). 	17

Figure 1.12 : Mechanism of coupling agent between hydrophilic fiber and hydrophobic 	21

Figure 3.1 :  Epoxy anhydride reaction in the absence of a catalyst.	61

Figure 3.2 :  Epoxy anhydride reaction in the presence of a catalyst.	61

Figure 3.3 : Schematic illustration of silane treated natural fibers.	67

Figure 3.4 :  Schematic illustration of FTIR system.	71

Figure 3.5 :   Nicolet 380 FTIR Spectrophotometer.	71

Figure 3.6 :  Thermogravimetric (TGA) Instrument.	75

Figure 3.7 :  Dynamic stress behaviour and material response.	75

Figure 3.8 :   Idealized temperatures scan of a polymer.	79

Figure 3.9 :   Perkin Elmer DMA 8000.	79

Figure 3.10 :  Flexural testing arrangement.	83

Figure 3.11 :  Notched Izod Impact strength Instrument.	83

Figure 3.12 :  SEM instrument and internal diagram.	87

Figure 4.1 :  Temperature dependence of loss factor tan δ for various ratios (R).	95

Figure 4.2 :  Glass transition temperature (Tg) and Peak factor as a function of R.	95

Figure 4.3 :  log f versus 1/T×1000.	97

Figure 4.4 :  Tg and activation energy (Ea) versus R.	97

Figure 4.5 :  Temperature dependence of the storage modulus E' for various ratios 	101

Figure 4.6 :  Tg and crosslink density (νe) with R.	101

Figure 4.7 :  Tensile strength and tensile modulus against R.	103

Figure 4.8 :  % Elongation at break and impact strength against R.	103

Figure 4.9 :  Flexural strength and flexural modulus against R.	105

Figure 4.10 : Impact failure surface of R = 0.7.	105

Figure 4.11 :  Impact failure surface of R = 1.0.	107

Figure 4.12 :  Impact failure surface of R = 1.3.	107

Figure 4.13 :  TGA thermograms of various ratios (R).	111

Figure 5.1 :  Tan δ curves versus temperature for different ESO/DGEBA systems.	117

Figure 5.2 :  Glass transition temperature (Tg) and Peak factor against DGEBA content	117

Figure 5.3 :  Storage modulus curves versus temperature for ESO/DGEBA systems.	119

Figure 5.4 :  Glass transition temperature and crosslink density versus DGEBA content.	119

Figure 5.5 :  Experimental and theoretical glass transition temperatures versus DGEBA 	123

Figure 5.6 :  Infrared spectrums of ESO/DGEBA systems.	123

Figure 5.7 :  Tensile strength and tensile modulus of ESO/DGEBA systems against 	125

Figure 5.8 :  % Elongation at break of ESO/DGEBA	125

Figure 5.9 :  Flexural strength and flexural modulus of ESO/DGEBA systems 	129

Figure 5.10 :  Impact strength of ESO/DGEBA systems against DGEBA content .	129

Figure 5.11 :  Impact fractured surface of neat ESO matrix.	131

Figure 5.12 :  Impact fractured surface of ESO/DGEBA (10). 	131

Figure 5.13 :  Impact fractured surface of ESO/DGEBA (20). 	133

Figure 5.14 :  Impact fractured surface of ESO/DGEBA (30). 	133

Figure 5.15 :  TGA curves for ESO/DGEBA systems with various DGEBA contents.	135

Figure 6.1 :  FTIR spectrum of untreated Sunhemp fiber.	143

Figure 6.2 :  FTIR spectrum of silane treated Sunhemp fiber.	143

Figure 6.3 :  TGA thermograms of (i) untreated and (ii) silane treated fibers.	145

Figure 6.4 :  SEM photograph of untreated Sunhemp fiber.	149

Figure 6.5 :  SEM photograph of silane treated Sunhemp fiber.	149

Figure 6.6 :  Tan δ for ESO-untreated sunhemp composites.	153

Figure 6.7 :  Tan δ for ESO-silane treated sunhemp composites.	153

Figure 6.8 :  Variation of Tg of ESO-untreated & silane treated composites with fiber content.	157

Figure 6.9 :  Variation of peak factor for ESO-untreated and silane treated 	157

Figure 6.10 :  Storage modulus (E') for ESO-untreated sunhemp composites.	159

Figure 6.11 :  Storage modulus (E') for ESO-silane treated sunhemp composites. 	159

Figure 6.12 :  Constant C for ESO-untreated and silane treated composites with fiber content.	163

Figure 6.13 :  Variation of crosslink density for ESO-untreated & silane treated 	163

Figure 6.14 :  Variation of tensile strength and tensile modulus for ESO-untreated 	165

Figure 6.15 :  Variation of tensile strength and tensile modulus for ESO-silane 	165

Figure 6.16 :  Variation of % Elongation at break for ESO-untreated & silane 	169

Figure 6.17 :  Variation of flexural strength and flexural modulus for ESO-untreated composites with fiber content.	169

Figure 6.18 :  Variation of flexural strength and flexural modulus for ESO-silane treated composites with fiber content.	171

Figure 6.19 :  Variation of Impact strength for ESO- untreated and silane treated composites with fiber content.	171

Figure 6.20 :  SEM micrograph of ESO-untreated fiber composite (0.5 wt %).	173

Figure 6.21 :  SEM of ESO-untreated fiber composites (1.5 wt %).	173

Figure 6.22 :  SEM image of ESO-untreated fiber composites (2.5 wt %).	175

Figure 6.23 :  SEM  showing improved adhesion of ESO-silane treated fibers (0.5wt %).	175

Figure 6.24 :  SEM  showing improved adhesion of ESO-silane treated fibers (1.5wt %).	177

Figure 6.25 :  SEM showing improved adhesion of ESO-silane treated fibers (2.5 wt %).	177

Figure 6.26 :  TGA curves for ESO untreated fiber composites with fiber content.	181

Figure 6.27 :  TGA curves for ESO silane treated fiber composites with fiber content.	181

Figure 6.28 :  Tan δ for ESO/DGEBA (10) untreated composites.	185

Figure 6.29 :  Tan δ for ESO/DGEBA (10) silane treated composites.	185

Figure 6.30 :  Variation of Tg of ESO/DGEBA (10) untreated & silane treated composites with fiber content.	187

Figure 6.31 :  Variation of peak factor for ESO/DGEBA (10) untreated and silane treated composites with fiber content.	187

Figure 6.32 :  Storage modulus (E') for ESO/DGEBA (10) untreated composites.	189

Figure 6.33 :  Storage modulus (E') for ESO/DGEBA (10) silane treated composites.	189

Figure 6.34 :  Constant C for ESO/DGEBA (10) untreated and silane treated composites with fiber content.	193

Figure 6.35 :  Variation of crosslink density for ESO/DGEBA (10) untreated & silane treated composites with fiber content.	193

Figure 6.36 :  Variation of tensile strength and tensile modulus for ESO/DGEBA (10) untreated composites with fiber content.	195

Figure 6.37 :  Variation of tensile strength and tensile modulus for ESO/DGEBA (10) silane treated composites with fiber content.	195

Figure 6.38 :  Variation of % Elongation at break for ESO/DGEBA (10) untreated & silane treated composites with fiber content.	199

Figure 6.39 :  Variation of flexural strength and flexural modulus for ESO/DGEBA (10) untreated composites with fiber content.	199

Figure 6.40 :  Variation of flexural strength and flexural modulus for ESO/DGEBA (10) silane treated composites with fiber content.	201

Figure 6.41 :  Variation of Impact strength for ESO/DGEBA (10) untreated and silane treated composites with fiber content.	201

Figure 6.42 :  SEM image showing untreated fiber (0.5wt. %) completely dissociated from the ESO/DGEBA (10) matrix.	203

Figure 6.43 :  SEM image showing untreated fiber (1.5wt. %) completely dissociated from the ESO/DGEBA (10) matrix.	203

Figure 6.44 :  SEM image showing untreated fiber (2.5wt. %) completely dissociated from the ESO/DGEBA (10) matrix.	205

Figure 6.45 :  SEM images showing improved adhesion of silane treated fibers (0.5 wt %) with ESO/DGEBA (10) matrix.	205

Figure 6.46 :  SEM images showing improved adhesion of silane treated fibers (1.5 wt %) with ESO/DGEBA (10) matrix.	207

Figure 6.47 :  SEM images showing improved adhesion of silane treated fibers (2.5 wt. %) with ESO/10 DGEBA matrix.	207

Figure 6.48 :  TGA curves for ESO/DGEBA (10) untreated fiber composites with fiber content.	211

Figure 6.49 :  TGA curves for ESO/DGEBA (10) silane treated fiber composites with fiber content.	211

List of Tables

Table 1.1 : Fatty acids in common oils.	5

Table 1.2 : Fatty acid distribution in various plant oils.	6

Table 1.3 : Chemical composition of various types of natural fibers.	15

Table 1.4: Crystallinity and microfibrillar angle of various natural fibers 	18

Table 1.5: Characteristic of representative commercial silane coupling agents	22

Table 1.6:  Applications in different fields.	27

Table 3.1:  Formulations for different R values.	63

Table 3.2:  DGEBA modified ESO systems.	65

Table 3.3:  Composition of untreated and silane treated fiber composites. 	69

Table 4.1: Onset and endset temperatures for various ratios R.	109

Table 5.1:  IDT and T50 wt% values for ESO/DGEBA systems	128

Table 6.1: Percentage weight loss (5wt%, 50wt% and 80wt %) of untreated and silane treated sunhemp fibers. 	142

Table 6.2: Percentage weight loss of untreated sunhemp fiber composites at 5wt%, 50wt% and 80wt%.	179

Table 6.3: Percentage weight loss of silane treated sunhemp fiber composites at 5wt%, 50wt% and 80wt%.	179

Table 6.4: Percentage weight loss of untreated sunnhemp fiber DGEBA (10) composites at 5wt%, 50wt% and 80wt%.	209

Table 6.5: Percentage weight loss of untreated sunnhemp fiber DGEBA (10) composites at 5wt%, 50wt% and 80wt%.	209

List of Abbreviations & Symbols

ASTM	American Society for the Testing and Materials

DGEBA	Diglycidylether of Bisphenol-A based epoxy resin

DMA	Dynamic Mechanical Analysis

ESO	Epoxidized Soybean Oil

FTIR	Fourier Transform Infrared Spectroscopy

HBr	Hydrogen bromide

HAc	Acetic acid

ISO	International Organization for Standardization

Pry	Pyridine

R	Stoichiometric ratio

RH	Relative humidity

SEM	Scanning Electron Microscopy (SEM)

TGA	Thermogravimetric Analysis

Tg	Glass transition temperature

σ 	Tensile Strength

%T 	Transmittance

I	Intensity

A	Absorbance.

ε 	Strain

E’	Storage Modulus

E’’	Loss Modulus

Tan δ	Loss factor

F	load

b	Width of the sample

h   	Thickness of the sample

Δl 	Extension

l0 	Initial Gauge Length

Et 	Young's Modulus in Tension

σf 	Stress in the Outer Specimen at Midpoint

P 	Load at a given point on the load deflection curve

L 	Support span

d 	Depth

EB	Modulus of Elasticity in Bending

m 	Slope of the tangent

Ea	Activation Energy

R	Gas Constant

Dedicated to my Parents